NATIONAL ANNEX

TO

CYS EN 1992-4:2018

Eurocode 2: Design of concrete structures

Part 4: Design of fastenings for use in concrete

Public Enquiry Draft

Period of Enquiry

Prepared by: CYS TC18 EUROCODES COMMITTEE

Cyprus Organisation for Standardisation

INTRODUCTION

This National Annex has been prepared by CYS TC 18 Standardisation Technical Committee of Cyprus Organisation for standardisation.

# SCOPE

This National Annex is to be used together with CYS EN 1992-4:2018. Any reference in the rest of this text to CYS EN 1992-4:2018 means the above document.

This National Annex gives:

Nationally determined parameters for the following clauses of CYS EN 1992-4:2018 where National choice is allowed (see Section NA 2)

- 4.4.1 (2)

- 4.4.2.2 (2)

- 4.4.2.3

- 4.4.2.4

- 4.7 (2)

- 9.3 (1)

- C.2 (2)

- C.4.4 (1)

- C.4.4 (3)

- D.2 (2)

Decisions on the use of the Informative Annexes A, B, C, D, E, F and G (see Section NA 3)

References to non-contradictory complementary information to assist the user to apply CYS EN 1992-4:2018.  In this National Annex such information is provided for the following clauses in CYS EN 1992-4:2018 (see Section NA 4)

# NATIONALLY DETERMINED PARAMETERS

## Clause 4.4.1 (2) Partial factors for actions

The values of partial factors for ultimate limit state are  for concrete failure and  for other modes of failure, and in case of fatigue loading.

## Clause 4.4.2.2 (2) Ultimate limit state (static, quasi static and seismic loading)

The value of a partial factor under static, quasi static, seismic and accidental loading is given in Table 4.1 (CYS), when the partial factor is not product dependent.

Table 4.1 (CYS): Values of partial factors

| Failure modes | Partial factor |
| --- | --- |
|  | Permanent and transient design situations | Accidental design situation |
| Steel failure – fasteners |
| Tension | γMs | = 1,2 ⋅ fuk/fyk ≥ 1,4 | = 1,05 ⋅ fuk/fyk ≥ 1,25 |
| Shear with and without lever arm |  | = 1,0 ⋅ fuk/fyk ≥ 1,25 when fuk ≤ 800 N/mm2 and fyk/fuk ≤ 0,8 | = 1,0 ⋅ fuk/fyk ≥ 1,25 when fuk ≤ 800 N/mm2 and fyk/fuk ≤ 0,8 |
|  |  | = 1,5 when fuk > 800 N/mm2 or fyk/fuk > 0,8 | = 1,3 when fuk > 800 N/mm2 or fyk/fuk > 0,8 |
| Steel failure – anchor channels |
| Tension in anchors and channel bolts | γMs | = 1,2 ⋅ fuk/fyk ≥ 1,4 | = 1,05 ⋅ fuk/fyk ≥ 1,25 |
| Shear with and without lever arm in channel bolts |  | = 1,0 ⋅ fuk/fyk ≥ 1,25 when fuk ≤ 800 N/mm2 and fyk/fuk ≤ 0,8 | = 1,0 ⋅ fuk/fyk ≥ 1,25 when fuk ≤ 800 N/mm2 and fyk/fuk ≤ 0,8 |
|  |  | = 1,5 when fuk > 800 N/mm2 or fyk/fuk > 0,8 | = 1,3 when fuk > 800 N/mm2 or fyk/fuk > 0,8 |
| Connection between anchor and channel in tension and shear | γMs,ca | = 1,8 | = 1,6 |
| Local failure of anchor channel by bending of lips in tension and shear | γMs,l | = 1,8 | = 1,6 |
| Bending of channel | γMs,flex | = 1,15 | = 1,0 |
| Steel failure – supplementary reinforcement |
| Tension | γMs,re | = 1,15 a | = 1,0 |
| Concrete related failure |
| Concrete cone failure, concrete edge failure, concrete blow-out failure, concrete pry-out failure | γMc | = γc ⋅ γinst | = γc ⋅ γinst |
|  | γc | = 1,5a for seismic repair and strengthening of existing structures see the CYS EN 1998 series | = 1,2a for seismic repair and strengthening of existing structures see the CYS EN 1998 series |
|  | γinst | = 1,0 for headed fasteners and anchor channels satisfying the requirements of 4.6 (in tension and shear) ≥ 1,0 for post-installed fasteners in tension, see relevant European Technical Product Specification = 1,0 for post-installed fasteners in shear |
| Concrete splitting failure | γMsp | = γMc |
| Pull-out and combined pull-out and concrete failure | γMp | = γMc |
| a The values are in accordance with CYS EN 1992-1-1. |

The values of partial factors, in Table 4.1 (CYS), take into account that the characteristic resistance for steel failure is based on fuk, except fyk should be used for bending of the channel of anchor channels and steel failure of supplementary reinforcement.

## Clause 4.4.2.3 Ultimate limit state (fatigue loading)

The values of the partial factors for material for fastenings under fatigue loading are  (steel failure) and  (concrete related failure modes).

## Clause 4.4.2.4 Serviceability limit state

The value of the partial factor for serviceability limit state is.

## Clause 4.7 (2) Determination of concrete condition

The value of the admissible tensile stress  for the definition of uncracked concrete is   N/mm2 and is based on the characteristic combination of loading at the serviceability limit state.

## Clause 9.3 (1) Derivation of forces acting on fasteners

The determination of seismic action effects may be found in NA to CYS EN1998-1:2004

# DECISION ON USE OF THE ANNEXES

## Annex A

Annex A may be used

## Annex B

Annex B may be used

## Annex C

Annex C may be used

## Annex C.2 (2) Performance categories

The assignment of the seismic performance categories C1 and C2 to the seismicity level and building importance classes are shown in Table C.1 (CYS).

Table C.1 (CYS): Seismic Performance categories for fasteners

| Seismicity levela | Importance Class acc. to CYS EN 1998-1:2004, 4.2.5 |
| --- | --- |
| Class |  | I | II | III | IV |
| Very Lowb |  | No seismic performance category required |
| Lowb |  | C1 | C1d or C2e | C2 |
| low |  | C1 | C2 |
| a The values defining the seismicity levels are in the NA to CYS EN 1992-4:2018. The recommended values are given here. b Definition according to CYS EN 1998-1:2004, 3.2.1. c = design ground acceleration on type A ground (see CYS EN 1998-1:2004, 3.2.1), S = soil factor (see CYS EN 1998-1:2004, 3.2.2). d C1 for fixing non-structural elements to structures (Type 'B' connections). e C2 for fixing structural elements to structures (Type 'A' connections). |

## Annex C.4.4 (1) Additions and alterations to EN 1998-1:2004, 4.3.5.2

The determination of the seismic action effects of non-structural elements can be determined applying Formula (4.24) of CYS EN 1998-1:2004 in combination with Formula (C.3) of CYS EN 1992-4:2018.

## Annex C.4.4 (3) Additions and alterations to EN 1998-1:2004, 4.3.5.2

The determination of the vertical seismic action effects of non-structural elements can be determined applying Formula C.5 of CYS EN 1992-4:2018.

## Annex D

Annex D may be used

## Annex D.2 (2) Partial factors

The value of the partial factor for materials  may be found in the CYS EN 1992-4:2018.

## Annex E

Annex E may be used

## Annex F

Annex F may be used

## Annex G

Annex G may be used

# REFERENCES TO NON-CONTRADICTORY COMPLEMENTARY INFORMATION

None