NATIONAL ANNEX

TO

CYS EN 1993-1-10: 2005/AC:2009) Eurocode 3:  Design of steel structures

Part 1-10:  Material toughness and through-thickness properties

DRAFT FOR PUBLIC ENQUIRY

Prepared by: CYS/TC18 EUROCODES COMMITTEE

Cyprus Organization of Standardization

INTRODUCTION

This National Annex has been prepared by CYS/TC18Committee of the Cyprus Organization of Standardization.

# SCOPE

This National Annex is to be used together with CYS EN 1993-1-10: 2005 (Including Corrigendum AC:2009). Any reference in the rest of this text to CYS EN 1993-1-10:2005 means the above document.

.

This National Annex gives:

Nationally determined parameters for the following clauses of CYS EN 1993-1-10: 2005  where National choice is allowed (see Section NA 2):

2.2(5)

3.1(1)

References to non-contradictory complementary information to assist the user to apply CYS EN 1993-1-10: 2005(see Section NA 3).

# NATIONALLY DETERMINED PARAMETERS

## Clause 2.2(5) Procedure

The safety element ΔTR to adjust TEd to other reliability requirements shall be taken ΔTR = 0 °C, when using the tabulated values according to 2.3 of CYS EN 1993-1-10: 2005.

Maximum values of the range between TEd and the test temperature and also the range of (Ed, to which the validity of values for permissible thicknesses shall be as shown in Table 2.1 (CYS) of CYS EN 1993-1-10: 2005.

The application of Table 2.1 (CYS) is extended to all steel grades shown in the table.

Table 2.1 (CYS): Maximum permissible values of element thickness t in mm

| Steel grade | Sub-grade | Charpy energy CVN | Reference temperature TEd [°C] |
| --- | --- | --- | --- |
|  |  |  | 10 | 0 | -10 | -20 | -30 | -40 | -50 | 10 | 0 | -10 | -20 | -30 | -40 | -50 | 10 | 0 | -10 | -20 | -30 | -40 | -50 |
|  |  | at T [°C] | Jmin | (Ed = 0,75 fy(t) | (Ed = 0,50 fy(t) | (Ed = 0,25 fy(t) |
| S235 | JR | 20 | 27 | 60 | 50 | 40 | 35 | 30 | 25 | 20 | 90 | 75 | 65 | 55 | 45 | 40 | 35 | 135 | 115 | 100 | 85 | 75 | 65 | 60 |
|  | J0 | 0 | 27 | 90 | 75 | 60 | 50 | 40 | 35 | 30 | 125 | 105 | 90 | 75 | 65 | 55 | 45 | 175 | 155 | 135 | 115 | 100 | 85 | 75 |
|  | J2 | -20 | 27 | 125 | 105 | 90 | 75 | 60 | 50 | 40 | 170 | 145 | 125 | 105 | 90 | 75 | 65 | 200 | 200 | 175 | 155 | 135 | 115 | 100 |
| S275 | JR | 20 | 27 | 55 | 45 | 35 | 30 | 25 | 20 | 15 | 80 | 70 | 55 | 50 | 40 | 35 | 30 | 125 | 110 | 95 | 80 | 70 | 60 | 55 |
|  | J0 | 0 | 27 | 75 | 65 | 55 | 45 | 35 | 30 | 25 | 115 | 95 | 80 | 70 | 55 | 50 | 40 | 165 | 145 | 125 | 110 | 95 | 80 | 70 |
|  | J2 | -20 | 27 | 110 | 95 | 75 | 65 | 55 | 45 | 35 | 155 | 130 | 115 | 95 | 80 | 70 | 55 | 200 | 190 | 165 | 145 | 125 | 110 | 95 |
|  | M,N | -20 | 40 | 135 | 110 | 95 | 75 | 65 | 55 | 45 | 180 | 155 | 130 | 115 | 95 | 80 | 70 | 200 | 200 | 190 | 165 | 145 | 125 | 110 |
|  | ML,NL | -50 | 27 | 185 | 160 | 135 | 110 | 95 | 75 | 65 | 200 | 200 | 180 | 155 | 130 | 115 | 95 | 230 | 200 | 200 | 200 | 190 | 165 | 145 |
| S355 | JR | 20 | 27 | 40 | 35 | 25 | 20 | 15 | 15 | 10 | 65 | 55 | 45 | 40 | 30 | 25 | 25 | 110 | 95 | 80 | 70 | 60 | 55 | 45 |
|  | J0 | 0 | 27 | 60 | 50 | 40 | 35 | 25 | 20 | 15 | 95 | 80 | 65 | 55 | 45 | 40 | 30 | 150 | 130 | 110 | 95 | 80 | 70 | 60 |
|  | J2 | -20 | 27 | 90 | 75 | 60 | 50 | 40 | 35 | 25 | 135 | 110 | 95 | 80 | 65 | 55 | 45 | 200 | 175 | 150 | 130 | 110 | 95 | 80 |
|  | K2,M,N | -20 | 40 | 110 | 90 | 75 | 60 | 50 | 40 | 35 | 155 | 135 | 110 | 95 | 80 | 65 | 55 | 200 | 200 | 175 | 150 | 130 | 110 | 95 |
|  | ML,NL | -50 | 27 | 155 | 130 | 110 | 90 | 75 | 60 | 50 | 200 | 180 | 155 | 135 | 110 | 95 | 80 | 210 | 200 | 200 | 200 | 175 | 150 | 130 |
| S420 | M,N | -20 | 40 | 95 | 80 | 65 | 55 | 45 | 35 | 30 | 140 | 120 | 100 | 85 | 70 | 60 | 50 | 200 | 185 | 160 | 140 | 120 | 100 | 85 |
|  | ML,NL | -50 | 27 | 135 | 115 | 95 | 80 | 65 | 55 | 45 | 190 | 165 | 140 | 120 | 100 | 85 | 70 | 200 | 200 | 200 | 185 | 160 | 140 | 120 |
| S460 | Q | -20 | 30 | 70 | 60 | 50 | 40 | 30 | 25 | 20 | 110 | 95 | 75 | 65 | 55 | 45 | 35 | 175 | 155 | 130 | 115 | 95 | 80 | 70 |
|  | M,N | -20 | 40 | 90 | 70 | 60 | 50 | 40 | 30 | 25 | 130 | 110 | 95 | 75 | 65 | 55 | 45 | 200 | 175 | 155 | 130 | 115 | 95 | 80 |
|  | QL | -40 | 30 | 105 | 90 | 70 | 60 | 50 | 40 | 30 | 155 | 130 | 110 | 95 | 75 | 65 | 55 | 200 | 200 | 175 | 155 | 130 | 115 | 95 |
|  | ML,NL | -50 | 27 | 125 | 105 | 90 | 70 | 60 | 50 | 40 | 180 | 155 | 130 | 110 | 95 | 75 | 65 | 200 | 200 | 200 | 175 | 155 | 130 | 115 |
|  | QL1 | -60 | 30 | 150 | 125 | 105 | 90 | 70 | 60 | 50 | 200 | 180 | 155 | 130 | 110 | 95 | 75 | 215 | 200 | 200 | 200 | 175 | 155 | 130 |
| S690 | Q | 0 | 40 | 40 | 30 | 25 | 20 | 15 | 10 | 10 | 65 | 55 | 45 | 35 | 30 | 20 | 20 | 120 | 100 | 85 | 75 | 60 | 50 | 45 |
|  | Q | -20 | 30 | 50 | 40 | 30 | 25 | 20 | 15 | 10 | 80 | 65 | 55 | 45 | 35 | 30 | 20 | 140 | 120 | 100 | 85 | 75 | 60 | 50 |
|  | QL | -20 | 40 | 60 | 50 | 40 | 30 | 25 | 20 | 15 | 95 | 80 | 65 | 55 | 45 | 35 | 30 | 165 | 140 | 120 | 100 | 85 | 75 | 60 |
|  | QL | -40 | 30 | 75 | 60 | 50 | 40 | 30 | 25 | 20 | 115 | 95 | 80 | 65 | 55 | 45 | 35 | 190 | 165 | 140 | 120 | 100 | 85 | 75 |
|  | QL1 | -40 | 40 | 90 | 75 | 60 | 50 | 40 | 30 | 25 | 135 | 115 | 95 | 80 | 65 | 55 | 45 | 200 | 190 | 165 | 140 | 120 | 100 | 85 |
|  | QL1 | -60 | 30 | 110 | 90 | 75 | 60 | 50 | 40 | 30 | 160 | 135 | 115 | 95 | 80 | 65 | 55 | 200 | 200 | 190 | 165 | 140 | 120 | 100 |

## Clause 3.1(1) General

(1)	The choice of quality class should be selected from Table 3.1 (CYS) of CYS EN 1993-1-10: 2005 depending on the consequences of lamellar tearing.

Table 3.1 (CYS): Choice of quality class according to CYS EN 10164

| Class | Application of guidance |
| --- | --- |
| 1 | All steel products and all thicknesses listed in European standards for all applications |
| 2 | Certain steel products and thicknesses listed in European standards and/or certain listed applications |

The recommended class 1 shall be used.

# REFERENCES TO NON-CONTRADICTORY COMPLEMENTARY INFORMATION

None