NATIONAL ANNEX

TO

CYS EN 1993-1-1:2005/A1:2014/AC:2009

Eurocode 3: Design of steel structures

Part 1-1: General rules and rules for buildings

DRAFT FOR PUBLIC ENQUIRY

Prepared by: CYS/TC18 EUROCODES COMMITTEE

Cyprus Organisation of Standardisation

INTRODUCTION

This National Annex has been prepared by the CYS/TC18 Committee of the Cyprus Organisation of Standardisation.

# SCOPE

This National Annex is to be used in conjunction with CYS EN 1993-1-1:2005 (Including Corrigendum AC:2009 and Amendment A1:2014). Any reference in the rest of this text to CYS EN 1993-1-1:2005 means the above document.

This National Annex gives:

Nationally Determined Parameters described in the following clauses of CYS EN 1993-1-1:2005 (see Section NA 2):

2.3.1 (1)

3.1 (2)

3.2.1 (1)

3.2.2 (1)

3.2.3 (1)P

3.2.3 (3)B

3.2.4 (1)B

5.2.1 (3)

5.2.2 (8)

5.3.2 (3)

5.3.2 (11)

5.3.4 (3)

6.1(1)

6.1 (1)B

6.3.2.2 (2)

6.3.2.3 (1)

6.3.2.3 (2)

6.3.2.4 (1)B

6.3.2.4 (2)B

6.3.3 (5)

6.3.4 (1)

7.2.1 (1)B

7.2.2 (1)B

7.2.3 (1)B

BB.1.3 (3)B

C.2.2 (3)

C.2.2 (4)

Decisions on the use of CYS EN 1993-1-1:2005 informative annexes (see Section NA 3)

References to non-contradictory complementary information to assist the user to apply CYS EN 1993-1-1:2005 (see Section NA 4)

# NATIONALLY DETERMINED PARAMETERS

## Clause 2.3.1 (1) Actions and environmental influences

Refer to the parts of CYS EN 1991 (including the respective Corrigenda and Amendments) and their National Annexes.

## Clause 3.1 (2) General

Refer to CYS EN 1993-1-12:2007/AC:2009 and its National Annex. No information for other steel material and products is provided in this National Annex.

## Clause 3.2.1 (1) Material properties

The nominal values of the yield strength fy and the ultimate strength fu for structural steel shall be obtained by adopting the values fy = ReH and fu = Rm direct from the product standard.

## Clause 3.2.2 (1) Ductility requirements

The following recommended requirements shall be used:

- fu / fy  (  1,10;

- elongation at failure not less than 15%;

- (u ( 15(y , where (y is the yield strain ((y = fy / E).

## Clause 3.2.3 (1)P Fracture toughness

Refer to CYS EN 1991-1-5:2003/AC:2009 and its National Annex.

## Clause 3.2.3 (3)B Fracture toughness

The toughness properties for members in compression shall be taken from Table 2.1 (CYS) of the CYS EN 1993-1-10:2005/AC:2009 for (Ed = 0,25 fy(t), which is repeated here.

Table 2.1 (CYS): Maximum permissible values of element thickness t in mm

| Steel grade | Sub-grade | Charpy energy CVN | Reference temperature TEd [°C] |
| --- | --- | --- | --- |
|  |  |  | 10 | 0 | -10 | -20 | -30 | -40 | -50 | 10 | 0 | -10 | -20 | -30 | -40 | -50 | 10 | 0 | -10 | -20 | -30 | -40 | -50 |
|  |  | at T [°C] | Jmin | (Ed = 0,75 fy(t) | (Ed = 0,50 fy(t) | (Ed = 0,25 fy(t) |
| S235 | JR | 20 | 27 | 60 | 50 | 40 | 35 | 30 | 25 | 20 | 90 | 75 | 65 | 55 | 45 | 40 | 35 | 135 | 115 | 100 | 85 | 75 | 65 | 60 |
|  | J0 | 0 | 27 | 90 | 75 | 60 | 50 | 40 | 35 | 30 | 125 | 105 | 90 | 75 | 65 | 55 | 45 | 175 | 155 | 135 | 115 | 100 | 85 | 75 |
|  | J2 | -20 | 27 | 125 | 105 | 90 | 75 | 60 | 50 | 40 | 170 | 145 | 125 | 105 | 90 | 75 | 65 | 200 | 200 | 175 | 155 | 135 | 115 | 100 |
| S275 | JR | 20 | 27 | 55 | 45 | 35 | 30 | 25 | 20 | 15 | 80 | 70 | 55 | 50 | 40 | 35 | 30 | 125 | 110 | 95 | 80 | 70 | 60 | 55 |
|  | J0 | 0 | 27 | 75 | 65 | 55 | 45 | 35 | 30 | 25 | 115 | 95 | 80 | 70 | 55 | 50 | 40 | 165 | 145 | 125 | 110 | 95 | 80 | 70 |
|  | J2 | -20 | 27 | 110 | 95 | 75 | 65 | 55 | 45 | 35 | 155 | 130 | 115 | 95 | 80 | 70 | 55 | 200 | 190 | 165 | 145 | 125 | 110 | 95 |
|  | M,N | -20 | 40 | 135 | 110 | 95 | 75 | 65 | 55 | 45 | 180 | 155 | 130 | 115 | 95 | 80 | 70 | 200 | 200 | 190 | 165 | 145 | 125 | 110 |
|  | ML,NL | -50 | 27 | 185 | 160 | 135 | 110 | 95 | 75 | 65 | 200 | 200 | 180 | 155 | 130 | 115 | 95 | 230 | 200 | 200 | 200 | 190 | 165 | 145 |
| S355 | JR | 20 | 27 | 40 | 35 | 25 | 20 | 15 | 15 | 10 | 65 | 55 | 45 | 40 | 30 | 25 | 25 | 110 | 95 | 80 | 70 | 60 | 55 | 45 |
|  | J0 | 0 | 27 | 60 | 50 | 40 | 35 | 25 | 20 | 15 | 95 | 80 | 65 | 55 | 45 | 40 | 30 | 150 | 130 | 110 | 95 | 80 | 70 | 60 |
|  | J2 | -20 | 27 | 90 | 75 | 60 | 50 | 40 | 35 | 25 | 135 | 110 | 95 | 80 | 65 | 55 | 45 | 200 | 175 | 150 | 130 | 110 | 95 | 80 |
|  | K2,M,N | -20 | 40 | 110 | 90 | 75 | 60 | 50 | 40 | 35 | 155 | 135 | 110 | 95 | 80 | 65 | 55 | 200 | 200 | 175 | 150 | 130 | 110 | 95 |
|  | ML,NL | -50 | 27 | 155 | 130 | 110 | 90 | 75 | 60 | 50 | 200 | 180 | 155 | 135 | 110 | 95 | 80 | 210 | 200 | 200 | 200 | 175 | 150 | 130 |
| S420 | M,N | -20 | 40 | 95 | 80 | 65 | 55 | 45 | 35 | 30 | 140 | 120 | 100 | 85 | 70 | 60 | 50 | 200 | 185 | 160 | 140 | 120 | 100 | 85 |
|  | ML,NL | -50 | 27 | 135 | 115 | 95 | 80 | 65 | 55 | 45 | 190 | 165 | 140 | 120 | 100 | 85 | 70 | 200 | 200 | 200 | 185 | 160 | 140 | 120 |
| S460 | Q | -20 | 30 | 70 | 60 | 50 | 40 | 30 | 25 | 20 | 110 | 95 | 75 | 65 | 55 | 45 | 35 | 175 | 155 | 130 | 115 | 95 | 80 | 70 |
|  | M,N | -20 | 40 | 90 | 70 | 60 | 50 | 40 | 30 | 25 | 130 | 110 | 95 | 75 | 65 | 55 | 45 | 200 | 175 | 155 | 130 | 115 | 95 | 80 |
|  | QL | -40 | 30 | 105 | 90 | 70 | 60 | 50 | 40 | 30 | 155 | 130 | 110 | 95 | 75 | 65 | 55 | 200 | 200 | 175 | 155 | 130 | 115 | 95 |
|  | ML,NL | -50 | 27 | 125 | 105 | 90 | 70 | 60 | 50 | 40 | 180 | 155 | 130 | 110 | 95 | 75 | 65 | 200 | 200 | 200 | 175 | 155 | 130 | 115 |
|  | QL1 | -60 | 30 | 150 | 125 | 105 | 90 | 70 | 60 | 50 | 200 | 180 | 155 | 130 | 110 | 95 | 75 | 215 | 200 | 200 | 200 | 175 | 155 | 130 |
| S690 | Q | 0 | 40 | 40 | 30 | 25 | 20 | 15 | 10 | 10 | 65 | 55 | 45 | 35 | 30 | 20 | 20 | 120 | 100 | 85 | 75 | 60 | 50 | 45 |
|  | Q | -20 | 30 | 50 | 40 | 30 | 25 | 20 | 15 | 10 | 80 | 65 | 55 | 45 | 35 | 30 | 20 | 140 | 120 | 100 | 85 | 75 | 60 | 50 |
|  | QL | -20 | 40 | 60 | 50 | 40 | 30 | 25 | 20 | 15 | 95 | 80 | 65 | 55 | 45 | 35 | 30 | 165 | 140 | 120 | 100 | 85 | 75 | 60 |
|  | QL | -40 | 30 | 75 | 60 | 50 | 40 | 30 | 25 | 20 | 115 | 95 | 80 | 65 | 55 | 45 | 35 | 190 | 165 | 140 | 120 | 100 | 85 | 75 |
|  | QL1 | -40 | 40 | 90 | 75 | 60 | 50 | 40 | 30 | 25 | 135 | 115 | 95 | 80 | 65 | 55 | 45 | 200 | 190 | 165 | 140 | 120 | 100 | 85 |
|  | QL1 | -60 | 30 | 110 | 90 | 75 | 60 | 50 | 40 | 30 | 160 | 135 | 115 | 95 | 80 | 65 | 55 | 200 | 200 | 190 | 165 | 140 | 120 | 100 |

NOTE 1  Linear interpolation can be used in applying Table 2.1 (CYS). Most applications require σEd values between σEd = 0,75 fy(t) and σEd = 0,50 fy(t). σEd = 0,25 fy(t) is given for interpolation purposes. Extrapolations beyond the extreme values are not valid.

NOTE 2  For ordering products made of S 690 steels the TJ – values should be specified.

## Clause 3.2.4 (1)B Through-thickness properties

The allocation of target values ZEd according to 3.2(2) of CYS EN 1993-1-10:2005/AC:2009 to the quality class in CYS EN 10164 are given in Table 3.2 (CYS).

Table 3.2 (CYS): Choice of quality class according to CYS EN 10164

| Target value of ZEd according to CYS EN 1993-1-10:2005/AC:2009 | Required value of ZRd according to CYS EN 10164 |
| --- | --- |
| ZEd ≤ 10 | — |
| 10 < ZEd ≤ 20 | Z 15 |
| 20 < ZEd ≤ 30 | Z 25 |
| ZEd > 30 | Z 35 |

## Clause 5.2.1 (3) Effects of deformed geometry of the structure

The lower limit for (cr shall be the general limit set in the clause.

## Clause 5.2.2 (8) Structural stability of frames

No further information is provided in this National Annex.

## Clause 5.3.2 (3) Imperfections for global analysis of frames

The values of initial local bow imperfection, e0 / L, are specified in Table 5.1 (CYS).

Table 5.1 (CYS): Design value of initial local bow imperfection e0 / L for members

| Buckling curve according to Table 6.2 | elastic analysis | plastic analysis |
| --- | --- | --- |
|  | e0 / L | e0 / L |
| a0 | 1 / 350 | 1 / 300 |
| a | 1 / 300 | 1 / 250 |
| b | 1 / 250 | 1 / 200 |
| c | 1 / 200 | 1 / 150 |
| d | 1 / 150 | 1 / 100 |

## Clause 5.3.2 (11) Imperfections for global analysis of frames

No further information is provided in this National Annex.

## Clause 5.3.4 (3) Member imperfections

The value of k is 0,5.

## Clause 6.1 (1) General

For structures not covered by CYS EN 1993 Part 2 to Part 6 (including the respective Corrigenda and Amendments), the values for the partial factors (Mi shall be taken from CYS EN 1993-2:2006/AC:2009.

## Clause 6.1 (1)B General

The values for the partial factors (Mi for buildings are:

(M0 = 1,00

(M1 = 1,00

(M2 = 1,25

## Clause 6.3.2.2 (2) Lateral torsional buckling curves – General case

The values of imperfection factor (LT are defined in Table 6.3 (CYS).

Table 6.3 (CYS): Imperfection factors for lateral torsional buckling curves

| Buckling curve | a | b | c | d |
| --- | --- | --- | --- | --- |
| Imperfection factor (LT | 0,21 | 0,34 | 0,49 | 0,76 |

The specification of the symbols for the buckling curves are given in Table 6.4 (CYS).

Table 6.4 (CYS): Lateral torsional buckling curves for cross-sections using equation (6.56)

| Cross-section | Limits | Buckling curve |
| --- | --- | --- |
| Rolled I-sections | h/b ( 2 h/b > 2 | a b |
| Welded I-sections | h/b ( 2 h/b > 2 | c d |
| Other cross-sections | - | d |

## Clause 6.3.2.3 (1) Lateral torsional buckling curves for rolled sections or equivalent welded sections

The following recommended limitations shall be used:

(maximum value)

( = 0,75	(minimum value)

The specification of the symbols for the lateral torsional buckling curves are given in Table 6.5 (CYS).

Table 6.5 (CYS): Selection of lateral torsional buckling curve for cross sections using equation (6.57)

| Cross-section | Limits | Buckling curve |
| --- | --- | --- |
| Rolled I-sections | h/b ( 2 h/b > 2 | b c |
| Welded I-sections | h/b ( 2 h/b > 2 | c d |

## Clause 6.3.2.3 (2) Lateral torsional buckling curves for rolled sections or equivalent welded sections

The following recommended minimum values shall be used:

Table 6.6 (CYS) defines the values for the correction factor, kc, of Table 6.6 of CYS EN 1993-1-1:2005.

Table 6.6 (CYS):  Correction factors kc

| Moment distribution | kc |
| --- | --- |
| ( = 1 | 1,0 |
| -1 ( ( ( 1 |  |
|  | 0,94 |
|  | 0,90 |
|  | 0,91 |
|  | 0,86 |
|  | 0,77 |
|  | 0,82 |

## Clause 6.3.2.4 (1)B Simplified assessment methods for beams with restraints in buildings

The recommended limit value  shall be used, see 6.3.2.3 of CYS EN 1993-1-1:2005.

## Clause 6.3.2.4 (2)B Simplified assessment methods for beams with restraints in buildings

The value of  is 1,10.

## Clause 6.3.3 (5) Uniform members in bending and axial compression

Method 2 is preferred, but Method 1 may be used at the discretion of the designer.

## Clause 6.3.4 (1) General method for lateral and lateral torsional buckling of structural components

The method may be used at the discretion of the designer.

## Clause 7.2.1 (1)B Vertical deflections

With reference to Figure A1.1 (CYS) of CYS EN 1990:2002/A1:2005/AC:2010, which is repeated here, the recommended limits for vertical deflections are given in Table NA1.

Figure A1.1 (CYS) - Definitions of vertical deflections

Key :

| wc | Precamber in the unloaded structural member |
| --- | --- |
| w1 | Initial part of the deflection under permanent loads of the relevant combination of actions according to expressions (6.14a) to (6.16b) |
| w2 | Long-term part of the deflection under permanent loads |
| w3 | Additional part of the deflection due to the variable actions of the relevant combination of actions according to expressions (6.14a) to (6.16b) |
| wtot | Total deflection as sum of w1 , w2 , w3 |
| wmax | Remaining total deflection taking into account the precamber |

Table NA1:  Recommended limits for vertical deflections

| Design situation | Total deflection limits |
| --- | --- |
| Cantilevers | Length/180 |
| Beams carrying plaster or other brittle finish | Span/360 |
| Other beams (except purlins and sheeting rails) | Span/250 |
| Purlins and sheeting rails | To suit cladding |

## Clause 7.2.2 (1)B Horizontal deflections

With reference to Figure A1.2 of CYS EN 1990:2002/A1:2005/AC:2010, which is repeated here, the recommended limits for horizontal deflections are given in Table NA2.

Figure A1.2 (CYS) - Definition of horizontal displacements

Key :

| u | Overall horizontal displacement over the building height H |
| --- | --- |
| ui | Horizontal displacement over a storey height Hi |

Table NA2:  Recommended limits for horizontal deflections

| Design situation | Deflection limits |
| --- | --- |
| Tops of columns in single storey buildings, except portal frames | Height/300 |
| Columns in portal frame buildings, not supporting crane runways | To suit cladding |
| In each storey of a building with more than one storey | Storey height/300 |
| On the multistorey building as a whole | Building height/500 |

## Clause 7.2.3 (1)B Dynamic effects

The recommended limits for vibration of floors are given in Table NA3.

Table NA3:  Recommended limits for vibration of floors

| Design situation | Lowest natural frequency |
| --- | --- |
| Floors over which people walk regularly | 5 Hz |
| Floor which is jumped or danced on in a rhythmical manner | 9 Hz |

## Clause BB.1.3 (3)B Hollow sections as members

No further information is provided in this National Annex.

## Clause C.2.2 (3) Selection

The selection of execution class shall be based on either the required consequences class (CC) or the reliability class (RC) or both for any type of structure. The selection of execution class (EXC) should be based on Table C.1 (CYS).

Table C.1 (CYS) – Choice of execution class (EXC)

| Reliability Class (RC) or Consequences Class (CC) | Type of loading |
| --- | --- |
|  | Static, quasi-static or seismic DCLa | Fatigueb or seismic DCM or DCHa |
| RC3 or CC3 | EXC3c | EXC3c |
| RC2 or CC2 | EXC2 | EXC3 |
| RC1 or CC1 | EXC1 | EXC2 |
| a Seismic ductility classes are defined in CYS EN 1998-1:2004/A1:2013/AC:2009: Low=DCL; Medium=DCM; High=DCH. b See CYS EN 1993-1-9:2005/AC:2009 and its National Annex. c EXC4 may be specified for structures with extreme consequences of structural failure. |

## Clause C.2.2 (4) Selection

Regarding the choice of execution class in terms of types of components or details, as recommended, if EXC1 is selected for a structure, then EXC2 should apply to the following types of component:

a)	welded components manufactured from steel products of grade S355 and above;

b)	welded components essential for structural integrity that are assembled by welding on the construction site;

c)	welded components of CHS lattice girders requiring end profile cuts;

d)	components with hot forming during manufacturing or receiving thermic treatment during manufacturing.

# DECISION ON THE USE OF INFORMATIVE ANNEXES

## Annex A

Annex A may be used.

## Annex B

Annex B may be used.

## Annex AB

Annex AB may be used.

## Annex BB

Annex BB may be used.

# REFERENCES TO NON-CONTRADICTORY COMPLEMENTARY INFORMATION

None

# Comments

‘should’ is used in the text of the Eurocode, therefore it is not changed to ‘shall’.

‘should’ is used in the text of the Eurocode, therefore it is not changed to ‘shall’.