NATIONAL ANNEX

TO

CYS EN 1993-1-3:2006/AC:2009

Eurocode 3: Design of steel structures

Part 1-3: General rules - Supplementary rules for cold-formed members and sheeting

DRAFT FOR PUBLIC ENQUIRY

Prepared by: CYS/TC18 EUROCODES COMMITTEE

Cyprus Organisation of Standardisation

INTRODUCTION

This National Annex has been prepared by the CYS/TC18 Committee of the Cyprus Organisation of Standardisation.

# SCOPE

This National Annex is to be used in conjunction with CYS EN 1993-1-3:2006 (Including Corrigendum AC:2009). Any reference in the rest of this text to CYS EN 1993-1-3:2006 means the above document.

This National Annex gives:

Nationally Determined Parameters described in the following clauses of CYS EN 1993-1-3:2006 (see Section NA 2):

2 (3)P

2 (5)

3.1 (3) Note 1 and Note 2

3.2.4 (1)

5.3 (4)

8.3 (5)

8.3 (13), Table 8.1

8.3 (13), Table 8.2

8.3 (13), Table 8.3

8.3 (13), Table 8.4

8.4 (5)

8.5.1 (4)

9 (2)

10.1.1 (1)

10.1.4.2 (1)

A.1 (1), Note 2

A.1 (1), Note 3

A.6.4 (4)

E (1)

Decisions on the use of CYS EN 1993-1-3:2006 informative annexes (see Section NA 3)

References to non-contradictory complementary information to assist the user to apply CYS EN 1993-1-3:2006 (see Section NA 4)

# NATIONALLY DETERMINED PARAMETERS

## Clause 2 (3) P Basis of design

The values for the partial factors Mi for buildings are:

M0 = 1,00;

M1 = 1,00;

M2 = 1,25.

## Clause 2 (5) Basis of design

The value of M,ser is 1,00.

## Clause 3.1 (3) Note 1 and Note 2 General

For steel strip less than 3 mm thick conforming to CYS EN 10025, if the width of the original strip is greater than or equal to 600 mm, the characteristic values shall be equal to 0,9 times those given in Table 3.1a (CYS).

Examples for other steel materials and products that may conform to the requirements of this standard are given in Table 3.1b (CYS).

# Table 3.1a (CYS):  Nominal values of basic yield strength  fyb  and ultimate tensile strength  fu

| Type of steel | Standard | Grade | fyb N/mm2 | fu N/mm2 |
| --- | --- | --- | --- | --- |
| Hot rolled products of non-alloy structural steels. Part 2: Technical delivery conditions for non alloy structural steels | CYS EN 10025: Part 2 | S 235 S 275 S 355 | 235 275 355 | 360 430 510 |
| Hot-rolled products of structural steels. Part 3: Technical delivery conditions for normalized/normalized rolled weldable fine grain structural steels | CYS EN 10025: Part 3 | S 275 N S 355 N S 420 N S 460 N S 275 NL S 355 NL S 420 NL S 460 NL | 275 355 420 460 275 355 420 460 | 370 470 520 550 370 470 520 550 |
| Hot-rolled products of structural steels. Part 4: Technical delivery conditions for thermomechanical rolled weldable fine grain structural steels | CYS EN 10025: Part 4 | S 275 M S 355 M S 420 M S 460 M S 275 ML S 355 ML S 420 ML S 460 ML | 275 355 420 460 275 355 420 460 | 360 450 500 530 360 450 500 530 |

# Table 3.1b (CYS):  Nominal values of basic yield strength  fyb  and ultimate tensile strength  fu

| Cold reduced steel sheet of structural quality | ISO 4997 | CR 220 CR 250 CR 320 | 220 250 320 | 300 330 400 |
| --- | --- | --- | --- | --- |
| Continuous hot dip zinc coated carbon steel sheet of structural quality | CYS EN 10326 | S220GD+Z S250GD+Z S280GD+Z S320GD+Z S350GD+Z | 220 250 280 320 350 | 300 330 360 390 420 |
| Hot-rolled flat products made of high yield strength steels for cold forming. Part 2: Delivery conditions for thermomechanically rolled steels | CYS EN 10149: Part 2 | S 315 MC S 355 MC S 420 MC S 460 MC S 500 MC S 550 MC S 600 MC S 650 MC S 700 MC | 315 355 420 460 500 550 600 650 700 | 390 430 480 520 550 600 650 700 750 |
|  | CYS EN 10149: Part 3 | S 260 NC S 315 NC S 355 NC S 420 NC | 260 315 355 420 | 370 430 470 530 |
| Cold-rolled flat products made of high yield strength micro-alloyed steels for cold forming | CYS EN 10268 | H240LA H280LA H320LA H360LA H400LA | 240 280 320 360 400 | 340 370 400 430 460 |
| Continuously hot-dip coated strip and sheet of steels with higher yield strength for cold forming | CYS EN 10292 | H260LAD H300LAD H340LAD H380LAD H420LAD | 240 2) 280 2) 320 2) 360 2) 400 2) | 340 2) 370 2) 400 2) 430 2) 460 2) |
| Continuously hot-dipped zinc-aluminium (ZA) coated steel strip and sheet | CYS EN 10326 | S220GD+ZA S250GD+ZA S280GD+ZA S320GD+ZA S350GD+ZA | 220 250 280 320 350 | 300 330 360 390 420 |
| Continuously hot-dipped aluminium-zinc (AZ) coated steel strip and sheet | CYS EN 10326 | S220GD+AZ S250GD+AZ S280GD+AZ S320GD+AZ S350GD+AZ | 220 250 280 320 350 | 300 330 360 390 420 |
| Continuously hot-dipped zinc coated strip and sheet of mild steel for cold forming | CYS EN 10327 | DX51D+Z DX52D+Z DX53D+Z | 140 1) 140 1) 140 1) | 270 1) 270 1) 270 1) |

1) Minimum values of the yield strength and ultimate tensile strength are not given in the standard. For all steel grades a minimum value of  140 N/mm2 for  yield strength and  270 N/mm2 for ultimate tensile strength may be assumed.

2) The yield strength values given in the names of the materials correspond to transversal tension. The values for longitudinal tension are given in the table.

## Clause 3.2.4 (1) Thickness and thickness tolerances

The following recommended ranges of core thickness tcor shall be used:

- for sheeting and members:    0,45mm  (  tcor  (  15 mm

- for connections:                     0,45mm  (  tcor  (  4 mm,	see 8.1(2) of
CYS EN 1993-1-3:2006

## Clause 5.3 (4) Structural modeling for analysis

The recommended values e0/L = 1/600 for elastic analysis and e0/L = 1/500 for plastic analysis shall be used for sections assigned to LTB buckling curve a taken from 6.3.2.2 of CYS EN 1993-1-1:2005/A1:2014/AC:2009.

## Clause 8.3 (5) Connections with mechanical fasteners

The value of M2 is 1,25.

## Clause 8.3 (13), Table 8.1 Connections with mechanical fasteners

No further information is provided in this National Annex.

## Clause 8.3 (13), Table 8.2 Connections with mechanical fasteners

No further information is provided in this National Annex.

## Clause 8.3 (13), Table 8.3 Connections with mechanical fasteners

No further information is provided in this National Annex.

## Clause 8.3 (13), Table 8.4 Connections with mechanical fasteners

No further information is provided in this National Annex.

## Clause 8.4 (5) Spot welds

The value of M2 is 1,25.

## Clause 8.5.1 (4) General

The value of M2 is 1,25.

## Clause 9 (2) Design assisted by testing

No further information is provided in this National Annex.

## Clause 10.1.1 (1) General

No further information is provided in this National Annex.

## Clause 10.1.4.2 (1) Buckling resistance of free flange

The value of the reduction factor LT shall be determined from 6.3.2.3 of CYS EN 1993-1-1:2005/A1:2014/AC:2009 using buckling curve  b  (LT=0,34 ;  ; (=0,75) for the relative slenderness    given in 10.1.4.2 (2) of CYS EN 1993-1-3:2006.

## Clause A.1 (1), Note 2 General

No further information is provided in this National Annex.

## Clause A.1 (1), Note 3 General

No further information is provided in this National Annex.

## Clause A.6.4 (4) Design values

The values for the partial factors Mi shall be those chosen in the design by calculation given in section 2 or section 8 of CYS EN 1993-1-3:2006, unless other values result from the use of Annex D of CYS EN 1990:2002/A1:2005/AC:2010.

## Clause E (1) Simplified design for purlins

No further information is provided in this National Annex.

# DECISION ON THE USE OF INFORMATIVE ANNEXES

## Annex B

Annex B may be used

## Annex C

Annex C may be used

## Annex D

Annex D may be used

## Annex E

Annex E may be used

# REFERENCES TO NON-CONTRADICTORY COMPLEMENTARY INFORMATION

None