NATIONAL ANNEX

TO

CYS EN 1993-1-4:2006/A1:2015

Eurocode 3: Design of steel structures

Part 1-4: General rules – Supplementary rules for stainless steels

Draft for Public Enquiry

Prepared by: CYS/TC18 EUROCODES COMMITTEE

Cyprus Organisation of Standardisation

INTRODUCTION

This National Annex has been prepared by the CYS/TC18 Committee of the Cyprus Organisation of Standardisation.

# SCOPE

This National Annex is to be used in conjunction with CYS EN 1993-1-4:2006 (Including Amendment A1:2015). Any reference in the rest of this text to CYS EN 1993-1-4:2006 means the above document.

This National Annex gives:

Nationally Determined Parameters described in the following clauses of CYS EN 1993-1-4:2006 (see Section NA 2):

2.1.4 (2)

2.1.5 (1)

5.1 (2)

5.5 (1)

5.6 (2)

6.1 (2)

6.2 (3)

7 (1)

A.2 (8)

A.3, Table A.4

Decisions on the use of CYS EN 1993-1-4:2006 informative annexes (see Section NA 3)

References to non-contradictory complementary information to assist the user to apply CYS EN 1993-1-4:2006 (see Section NA 4)

# NATIONALLY DETERMINED PARAMETERS

## Clause 2.1.4 (2) Fracture toughness

No further information is provided in this National Annex.

## Clause 2.1.5 (1) Through-thickness properties

No further information is provided in this National Annex.

## Clause 5.1 (2) General

The values for the partial factors (M are:

(M0 = 1,1

(M1 = 1,1

(M2 = 1,25

## Clause 5.5 (1) Uniform members in bending and axial compression

The values for the interaction factors ky, kz, kLT are:

but

but

kLT=1,0

No other interaction formulae as alternatives to equations 5.13 to 5.17 of CYS EN 1993-1-4:2006 are provided in this National Annex.

## Clause 5.6 (2) Shear resistance

The value of ( is 1,20.

## Clause 6.1 (2) General

No further information is provided in this National Annex.

## Clause 6.2 (3) Bolted connections

The following recommended values of ( shall be used:

- if the shear plane passes through unthreaded portion of the bolt, (=0,6

- if the shear plane passes through the threaded portion of the bolt, (=0,5

## Clause 7 (1) Design assisted by testing

No further information is provided in this National Annex.

## Clause A.2 (8) Selection of materials

A less severe CRF may be chosen when validated local operating experience or test data support such a choice.

## Clause A.3, Table A.4 Swimming pool environments

No further information is provided in this National Annex.

# DECISION ON THE USE OF INFORMATIVE ANNEXES

## Annex B

Annex B may be used.

## Annex C

Annex C may be used.

# REFERENCES TO NON-CONTRADICTORY COMPLEMENTARY INFORMATION

None