NATIONAL ANNEX

TO

CYS EN 1993-2:2006+AC:2009

Eurocode 3: Design of steel structures

Part 2: Steel bridges

DRAFT FOR PUBLIC ENQUIRY

Prepared by: CYS TC 18 Eurocodes Committee

Cyprus Organisation for Standardisation

INTRODUCTION

This National Annex has been prepared by the CYS TC 18 Eurocodes Committee of the Cyprus Organisation for Standardisation

# SCOPE

This National Annex is to be used together with CYS EN 1993-2:2006+AC:2009. Any references  in the rest of this text to CYS EN 1993-2:2006+AC:2009 means the above document.

This National Annex gives:

Nationally determined parameters for the following clauses of CYS EN 1993-2:2006 where National choice is allowed (see Section NA 2)

2.1.3.2 (1)

2.1.3.3 (5)

2.1.3.4 (1) & (2)

2.3.1 (1)

3.2.3 (2) & (3)

3.2.4 (1)

3.4 (1)

3.5 (1)

3.6 (1) & (2)

4 (1) & (4)

5.2.1 (4)

5.4.1 (1)

6.1 (1)P

6.2.2.3 (1)

6.2.2.5 (1)

6.3.2.3 (1)

6.3.4.2 (1) & (7)

7.1 (5)

7.3 (1)

7.4 (1)

8.1.3.2.1 (1)

8.1.6.3 (1)

8.2.1.4 (1)

8.2.1.5 (1)

8.2.1.6 (1)

8.2.10 (1)

8.2.13 (1)

8.2.14 (1)

9.1.2 (1)

9.1.3 (1)

9.3 (1)P & (2)P

9.4.1 (6)

9.5.2 (2), (3), (5), (6) & (7)

9.5.3 (2) (2 places)

9.6 (1) (2 places)

9.7 (1)

A.3.3 (1)P

A.3.6 (2)

A.4.2.1 (2), (3) & (4)

A.4.2.4 (2)

C.1.1 (2)

C.1.2.2 (1) & (2)

E.2 (1)

Decisions on the use of the Informative Annexes A, B, C, D and E (see Section NA 3)

References to non-contradictory complementary information to assist the user to apply CYS EN 1993-2:2006.  In this National Annex such information is provided for the following clauses in CYS EN 1993-2:2006 (see Section NA 4)

# NATIONALLY DETERMINED PARAMETERS

## Clause 2.1.3.2 (1) Design working life

The recommended value of 100 years is adopted for the design working life of a permanent bridge.

## Clause 2.1.3.3 (5) Durability

No additional recommendations are provided for durable details.

## Clause 2.1.3.4 (1) Robustness and structural integrity

No recommendation is provided for components subject to accidental design situations.

## Clause 2.1.3.4 (2) Robustness and structural integrity

No recommendation is provided for the choice of a design method.

## Clause 2.3.1 (1)

No additional actions are specified beyond EN 1991.

## Clause 3.2.3 (2)

No additional requirements are specified for the toughness of the base material.

## Clause 3.2.3 (3)

Use Table 2.1 of EN 1993-1-10 for for σEd = 0,25fy(t) as recommended. The maximum permissible values of elements thickness t are specified in Table 2.1 of CYS EN 1993-1-10, which is repeated below.

Table 2.1: Maximum permissible values of element thickness t in mm

| Steel grade | Sub-grade | Charpy energy CVN | Reference temperature TEd [°C] |
| --- | --- | --- | --- |
|  |  |  | 10 | 0 | -10 | -20 | -30 | -40 | -50 | 10 | 0 | -10 | -20 | -30 | -40 | -50 | 10 | 0 | -10 | -20 | -30 | -40 | -50 |
|  |  | at T [°C] | Jmin | (Ed = 0,75 fy(t) | (Ed = 0,50 fy(t) | (Ed = 0,25 fy(t) |
| S235 | JR | 20 | 27 | 60 | 50 | 40 | 35 | 30 | 25 | 20 | 90 | 75 | 65 | 55 | 45 | 40 | 35 | 135 | 115 | 100 | 85 | 75 | 65 | 60 |
|  | J0 | 0 | 27 | 90 | 75 | 60 | 50 | 40 | 35 | 30 | 125 | 105 | 90 | 75 | 65 | 55 | 45 | 175 | 155 | 135 | 115 | 100 | 85 | 75 |
|  | J2 | -20 | 27 | 125 | 105 | 90 | 75 | 60 | 50 | 40 | 170 | 145 | 125 | 105 | 90 | 75 | 65 | 200 | 200 | 175 | 155 | 135 | 115 | 100 |
| S275 | JR | 20 | 27 | 55 | 45 | 35 | 30 | 25 | 20 | 15 | 80 | 70 | 55 | 50 | 40 | 35 | 30 | 125 | 110 | 95 | 80 | 70 | 60 | 55 |
|  | J0 | 0 | 27 | 75 | 65 | 55 | 45 | 35 | 30 | 25 | 115 | 95 | 80 | 70 | 55 | 50 | 40 | 165 | 145 | 125 | 110 | 95 | 80 | 70 |
|  | J2 | -20 | 27 | 110 | 95 | 75 | 65 | 55 | 45 | 35 | 155 | 130 | 115 | 95 | 80 | 70 | 55 | 200 | 190 | 165 | 145 | 125 | 110 | 95 |
|  | M,N | -20 | 40 | 135 | 110 | 95 | 75 | 65 | 55 | 45 | 180 | 155 | 130 | 115 | 95 | 80 | 70 | 200 | 200 | 190 | 165 | 145 | 125 | 110 |
|  | ML,NL | -50 | 27 | 185 | 160 | 135 | 110 | 95 | 75 | 65 | 200 | 200 | 180 | 155 | 130 | 115 | 95 | 230 | 200 | 200 | 200 | 190 | 165 | 145 |
| S355 | JR | 20 | 27 | 40 | 35 | 25 | 20 | 15 | 15 | 10 | 65 | 55 | 45 | 40 | 30 | 25 | 25 | 110 | 95 | 80 | 70 | 60 | 55 | 45 |
|  | J0 | 0 | 27 | 60 | 50 | 40 | 35 | 25 | 20 | 15 | 95 | 80 | 65 | 55 | 45 | 40 | 30 | 150 | 130 | 110 | 95 | 80 | 70 | 60 |
|  | J2 | -20 | 27 | 90 | 75 | 60 | 50 | 40 | 35 | 25 | 135 | 110 | 95 | 80 | 65 | 55 | 45 | 200 | 175 | 150 | 130 | 110 | 95 | 80 |
|  | K2,M,N | -20 | 40 | 110 | 90 | 75 | 60 | 50 | 40 | 35 | 155 | 135 | 110 | 95 | 80 | 65 | 55 | 200 | 200 | 175 | 150 | 130 | 110 | 95 |
|  | ML,NL | -50 | 27 | 155 | 130 | 110 | 90 | 75 | 60 | 50 | 200 | 180 | 155 | 135 | 110 | 95 | 80 | 210 | 200 | 200 | 200 | 175 | 150 | 130 |
| S420 | M,N | -20 | 40 | 95 | 80 | 65 | 55 | 45 | 35 | 30 | 140 | 120 | 100 | 85 | 70 | 60 | 50 | 200 | 185 | 160 | 140 | 120 | 100 | 85 |
|  | ML,NL | -50 | 27 | 135 | 115 | 95 | 80 | 65 | 55 | 45 | 190 | 165 | 140 | 120 | 100 | 85 | 70 | 200 | 200 | 200 | 185 | 160 | 140 | 120 |
| S460 | Q | -20 | 30 | 70 | 60 | 50 | 40 | 30 | 25 | 20 | 110 | 95 | 75 | 65 | 55 | 45 | 35 | 175 | 155 | 130 | 115 | 95 | 80 | 70 |
|  | M,N | -20 | 40 | 90 | 70 | 60 | 50 | 40 | 30 | 25 | 130 | 110 | 95 | 75 | 65 | 55 | 45 | 200 | 175 | 155 | 130 | 115 | 95 | 80 |
|  | QL | -40 | 30 | 105 | 90 | 70 | 60 | 50 | 40 | 30 | 155 | 130 | 110 | 95 | 75 | 65 | 55 | 200 | 200 | 175 | 155 | 130 | 115 | 95 |
|  | ML,NL | -50 | 27 | 125 | 105 | 90 | 70 | 60 | 50 | 40 | 180 | 155 | 130 | 110 | 95 | 75 | 65 | 200 | 200 | 200 | 175 | 155 | 130 | 115 |
|  | QL1 | -60 | 30 | 150 | 125 | 105 | 90 | 70 | 60 | 50 | 200 | 180 | 155 | 130 | 110 | 95 | 75 | 215 | 200 | 200 | 200 | 175 | 155 | 130 |
| S690 | Q | 0 | 40 | 40 | 30 | 25 | 20 | 15 | 10 | 10 | 65 | 55 | 45 | 35 | 30 | 20 | 20 | 120 | 100 | 85 | 75 | 60 | 50 | 45 |
|  | Q | -20 | 30 | 50 | 40 | 30 | 25 | 20 | 15 | 10 | 80 | 65 | 55 | 45 | 35 | 30 | 20 | 140 | 120 | 100 | 85 | 75 | 60 | 50 |
|  | QL | -20 | 40 | 60 | 50 | 40 | 30 | 25 | 20 | 15 | 95 | 80 | 65 | 55 | 45 | 35 | 30 | 165 | 140 | 120 | 100 | 85 | 75 | 60 |
|  | QL | -40 | 30 | 75 | 60 | 50 | 40 | 30 | 25 | 20 | 115 | 95 | 80 | 65 | 55 | 45 | 35 | 190 | 165 | 140 | 120 | 100 | 85 | 75 |
|  | QL1 | -40 | 40 | 90 | 75 | 60 | 50 | 40 | 30 | 25 | 135 | 115 | 95 | 80 | 65 | 55 | 45 | 200 | 190 | 165 | 140 | 120 | 100 | 85 |
|  | QL1 | -60 | 30 | 110 | 90 | 75 | 60 | 50 | 40 | 30 | 160 | 135 | 115 | 95 | 80 | 65 | 55 | 200 | 200 | 190 | 165 | 140 | 120 | 100 |

NOTE 1  Linear interpolation can be used in applying Table 2.1. Most applications require σEd values between σEd = 0,75 fy(t) and σEd = 0,50 fy(t). σEd = 0,25 fy(t) is given for interpolation purposes. Extrapolations beyond the extreme values are not valid.

NOTE 2  For ordering products made of S 690 steels, the test temperature TAV should be given.

NOTE 3  Table 2.1 has been derived for the guaranteed Charpy energy values CVN in the direction of the rolling of the product.

## Clause 3.2.4 (1)

The required quality classes according to EN10164 are specified in Table 3.2 (CYS).

Table 3.2:  Quality class conforming to EN 10164

| Target value ZEd | Quality class |
| --- | --- |
| ZEd ( 10 | – |
| 10 < ZEd ( 20 | Z15 |
| 20 < ZEd ( 30 | Z25 |
| ZEd > 30 | Z35 |

## Clause 3.4 (1)

No types of cables for specific bridge types are specified.

## Clause 3.5 (1)

No further guidance is provided.

## Clause 3.6 (1)

No further guidance is provided.

## Clause 3.6 (2)

No further guidance is provided.

## Clause 4 (1)

No further guidance is provided.

## Clause 4 (4)

No further guidance is provided.

## Clause 5.2.1 (4)

No further guidance is provided.

## Clause 5.4.1 (1)

No further guidance is provided.

## Clause 6.1 (1)P

The following recommended partial factors for γMi are specified as:

γM0 = 1,00

γM1 = 1,10

γM2 = 1,25

γM3 = 1,25

γM3,ser = 1,10

γM4 = 1,10

γM5 = 1,10

γM6,ser = 1,00

γM7 = 1,10

## Clause 6.2.2.3 (1)

No further guidance is provided.

## Clause 6.2.2.5 (1)

Both methods 1 and 2 may be used. No further guidance is provided for method 2.

## Clause 6.3.2.3 (1)

No further information is provided.

## Clause 6.3.4.2 (1)

The recommended values of  λc,0 is 0,2 and kfl is 1,0..

## Clause 6.3.4.2 (7)

No further guidance is provided.

## Clause 7.1 (5)

No further guidance is provided.

## Clause 7.3 (1)

The recommended value of γMser is 1,0.

## Clause 7.4 (1)

No further guidance is provided.

## Clause 8.1.3.2.1 (1)

No further guidance is provided.

## Clause 8.1.6.3 (1)

No further guidance is provided.

## Clause 8.2.1.4 (1)

No further guidance is provided.

## Clause 8.2.1.5 (1)

No further guidance is provided.

## Clause 8.2.1.6 (1)

No further guidance is provided.

## Clause 8.2.10 (1)

No further guidance is provided.

## Clause 8.2.13 (1)

No further guidance is provided.

## Clause 8.2.14 (1)

No further guidance is provided.

## Clause 9.1.2 (1)

No further guidance is provided.

## Clause 9.1.3 (1)

No further guidance is provided.

## Clause 9.3 (1)P

The recommended value of γFf is 1,0.

## Clause 9.3 (2)P

The recommended values of γMf are specified in Table 3.1 of CYS EN 1993-1-9and is repeated below.

Table 3.1: Recommended values for partial factors for fatigue strength

| Assessment method | Consequence of failure |
| --- | --- |
|  | Low consequence | High consequence |
| Damage tolerant | 1,00 | 1,15 |
| Safe life | 1,15 | 1,35 |

## Clause 9.4.1 (6)

No further guidance is provided.

## Clause 9.5.2 (2)

The recommended values of λ1 are specified in Figure 9.5 of CYS EN 1993-2 and is repeated below.

| span length L [m] | span length L [m] |
| --- | --- |
| at midspan | at support |

Figure 9.5:  λ1 for moments for road bridges

## Clause 9.5.2 (3)

No further guidance is provided.

## Clause 9.5.2 (5)

The recommended value of tLd is 100 years.

## Clause 9.5.2 (6)

No further guidance is provided.

## Clause 9.5.2 (7)

The recommended values of λmax are specified in Figure 9.6 of CYS EN 1993-2 and is repeated below.

| span length L [m] | span length L [m] |
| --- | --- |
| at midspan | at support |

## Figure 9.6:  λmax for moments for road bridgesClause 9.5.3 (2) (2 places)

Note 1: No further guidance is provided.

Note 3: No further guidance is provided.

## Clause 9.6 (1) (2 places)

Note 1: No details from EN 1993-1-9 are excluded for the design of bridges.

Note 2: No further guidance is provided.

## Clause 9.7 (1)

No further guidance is provided.

## Clause A.3.3 (1)P

The recommended value of γμ is 2,0 for steel on steel and γμ is 1,2 for steel on concrete.

## Clause A.3.6 (2)

The recommended values of a are specified in Table A.2 of CYS EN 1993-2 and is repeated below.

Table A.2:  Factors (

| n | ( |
| --- | --- |
| ( 4 | 1 |
| 4 < n < 10 |  |
| ( 10 | 0,5 |

## Clause A.4.2.1 (2)

No further guidance is provided.

## Clause A.4.2.1 (3)

The recommended values of ΔT0 are specified in Table A.4 of CYS EN 1993-2 and is repeated below.

Table A.4:  Numerical values for ΔT0

| Case | Installation of bearings | (T0 [°C] |
| --- | --- | --- |
| 1 | Installation with measured temperature and with correction by resetting | 0 |
| 2 | Installation with estimated temperature and without correction by resetting with bridge set at T0 ( 10 °C | 15 |
| 3 | Installation with estimated temperature and without correction by resetting and also one or more changes in the position of the fixed bearing | 30 |

## Clause A.4.2.1 (4)

The values of ΔT0 are specified in Table A.4 of CYS EN 1993-2 and is repeated above. The additional safety term is ΔTγ = ( 5 οC.

## Clause A.4.2.4 (2)

No further guidance is provided.

## Clause C.1.1 (2)

No further guidance is provided.

## Clause C.1.2.2 (1)

The recommended values for the plate dimensions appear in Note 1 and Figure C.2 of CYS EN 1993-2 and is repeated below.

|  | 1 wheel load |
| --- | --- |

Figure C.2:  Effect of a) local wheel loads and b) differential deflections of stiffeners

## Clause C.1.2.2 (2)

The recommended minimum stiffness values are specified in Figure C.4 of CYS EN 1993-2 and is repeated below.

| distance between cross girders a [m] |  |
| --- | --- |
|  | second moment of area IB of the stringers including deck plate [cm4] |

| Condition for curve A |
| --- |
|  | 1 traffic lane for heavy vehicles 2 web of main girder or longitudinal girder |

NOTE	a)	Curve A applies to all stiffeners, that are not covered by b).

b)	Curve B applies to stiffeners that are located under the most heavily loaded traffic lane within 1,20 m of a web of a main girder

c)	The figure applies to all types of stiffeners

Figure C.4:  Minimum stiffness of longitudinal stiffeners

## Clause E.2 (1) Combination factor

The recommended values of the combination factor ψ are shown in Figure E.2 of CYS EN 1993-2 and is repeated below.

Figure E.2:  Combination factor dependent on span length L

# DECISION ON USE OF THE INFORMATIVE ANNEXES A, B, C, D and E

## Annex A

Annex A may be used.

## Annex B

Annex B may be used.

## Annex C

Annex C may be used.

## Annex D

Annex D may be used.

## Annex E

Annex E may be used.

# REFERENCES TO NON-CONTRADICTORY COMPLEMENTARY INFORMATION

None

# Text boxes

1

0

2

0

3

0

4

0

5

0

6

0

7

0

8

0

1

,

0

1

,

2

1

,

4

1

,

6

1

,

8

2

,

0

2

,

2

2

,

4

2

,

6

2

,

8

3

,

0

3

,

2

3

,

4

2

,

5

5

-

0

,

7

l

-

1

0

7

0

s

p

a

n

l

e

n

g

t

h

L

[

m

]

1



2

,

5

5

1

,

8

5

1

t

a

b

)

a

)

e

L [m]

20

40

1,0

0,7

