NATIONAL ANNEX

TO

CYS EN 1993-5:2007/AC:2009 Eurocode 3: Design of steel structures

Part 5: Piling

DRAFT FOR PUBLIC ENQUIRY

Prepared by: CYS/TC18

Cyprus Organisation of Standardisation

INTRODUCTION

This National Annex has been prepared by the CYS/TC18 Committee of the Cyprus Organisation of Standardisation.

# SCOPE

This National Annex is to be used together with CYS EN 1993-5:2007

This National Annex gives:

Nationally determined parameters for the following clauses of CYS EN 1993-5:2007 where National choice is allowed (see Section NA 2)

3.7(1)

3.9(1)P

4.4(1)

5.1.1(4)

5.2.2(2)

5.2.2(13)

5.2.5(7)

5.5.4(2)

6.4(3)

7.1(4)

7.2.3(2)

7.4.2(4)

A.3.1(3)

B.5.4(1)

D.2.2(5)

Decisions on the use of the Informative Annexes B , C and D (see Section NA 3)

References to non-contradictory complementary information to assist the user to apply CYS EN 1993-5:2007 (see Section NA 4)

# NATIONALLY DETERMINED PARAMETERS

## Clause 3.7 (1) Steel members used for anchors

The value fy,spec,max  is specified as 500 N/mm² .

## Clause 3.9 (1)P  Fracture toughness

Refer to CYS EN1991-1-5 and its National Annex.

## Clause 4.4 (1) Corrosion rates for design

Suitable values for corrosion rates are given in Table 4-1 (CYS) and Table 4-2 (CYS).

Table 4-1 (CYS) :  Value for the loss of thickness [mm] due to corrosion for piles and sheet piles in soils, with or without groundwater

| Required design working life | 5 years | 25 years | 50 years | 75 years | 100 years |
| --- | --- | --- | --- | --- | --- |
| Undisturbed natural soils (sand, silt, clay, schist, ....) | 0,00 | 0,30 | 0,60 | 0,90 | 1,20 |
| Polluted natural soils and industrial sites | 0,15 | 0,75 | 1,50 | 2,25 | 3,00 |
| Aggressive natural soils (swamp, marsh, peat, ...) | 0,20 | 1,00 | 1,75 | 2,50 | 3,25 |
| Non-compacted and non-aggressive fills (clay, schist, sand, silt, ....) | 0,18 | 0,70 | 1,20 | 1,70 | 2,20 |
| Non-compacted and aggressive fills (ashes, slag, ....) | 0,50 | 2,00 | 3,25 | 4,50 | 5,75 |
| Notes: 1) Corrosion rates in compacted fills are lower than those in non-compacted ones. In compacted fills the figures in the table should be divided by two. 2) The values given for 5 and 25 years are based on measurements, whereas the other values are extrapolated. |

Table 4-2 (CYS) :  Value for the loss of thickness [mm] due to corrosion for piles and sheet piles in fresh water or in sea water

| Required design working life | 5 years | 25 years | 50 years | 75 years | 100 years |
| --- | --- | --- | --- | --- | --- |
| Common fresh water (river, ship canal, ....) in the zone of high attack (water line) | 0,15 | 0,55 | 0,90 | 1,15 | 1,40 |
| Very polluted fresh water (sewage, industrial effluent, ....) in the zone of high attack (water line) | 0,30 | 1,30 | 2,30 | 3,30 | 4,30 |
| Sea water in temperate climate in the zone of high attack (low water and splash zones) | 0,55 | 1,90 | 3,75 | 5,60 | 7,50 |
| Sea water in temperate climate in the zone of permanent immersion or in the intertidal zone | 0,25 | 0,90 | 1,75 | 2,60 | 3,50 |
| Notes: 1) The highest corrosion rate is usually found in the splash zone or at the low water level in tidal waters. However, in most cases, the highest bending stresses occur in the permanent immersion zone, see figure 4-1. 2) The values given for 5 and 25 years are based on measurements, whereas the other values are extrapolated. |

a) Vertical zoning of		b) Corrosion rate 		c) Typical bending

sea water aggressivity	     distribution at side		    moment distribution

exposed to sea water

A       Zone of high attack (splash zone); 	             B       Intertidal zone;

C       Zone of high attack (Low water zone);              D       Permanent immersion zone;

E       Buried zone (Water side); 			 F       Anchor;

G       Buried zone (Soil side)

MHW 	Mean high water; 				 MLW Mean low water

NOTE: Corrosion rate distribution and zones of sea water aggressivity may vary considerably from the example shown in Figure 4

Figure 2-1, dependant upon the conditions prevailing at the location of the structure.

Figure 2-1 (CYS): Example of corrosion rate distribution

## Clause 5.1.1 (4) Ultimate limit states - General

The values for the partial factors M0, M1 and M2 for piling are specified as : M0 = 1,00; M1 = 1,10 and M2 = 1,25.

## Clause 5.2.2 (2)  Sheet piling in bending and shear

The numerical value for βB for single and double U-piles is specified as 1,00 .

## Clause 5.2.2 (13)  Sheet piling in bending and shear

The value l  is specified as 500 mm .

## Clause 5.2.5 (7)  Straight web steel sheet piles

The recommended value βR = 0,8 shall be used .

## Clause 5.5.4 (2)  Primary elements

The recommended value  h = 5 m shall be used .

## Clause 6.4 (3)  Structural aspects of steel sheet piling

The numerical value for βD  is specified as 1,00 .

## Clause 7.1  Anchors, walings, bracing and connections -  General

The recommended values for the partial factors Mb = 1,25 and M3,ser = 1,10 shall be used.

## Clause 7.2.3 (2)    Anchorages -  Ultimate limit state verification

The recommended kt = 0,6 shall be used. This is motivated for cases where possible bending in the anchor as an effect of actions is not made explicit. Only in cases where the structural detailing of the location where the anchor rod is joined to the wall is such that bending moments are avoided at that location, the value for kt may be chosen as kt = 0,9.

## Clause 7.4.2.(4) Bearing piles

No further information on the design procedure for pile couplers is provided in this National Annex.

## Clause A.3.1(3)  Material properties

The following recommended limiting values shall be used:

- fu / fy ( 1,1;

- elongation at failure ( 15 %;

- u ( 15 y;

- where y corresponds to the yield strength fy;

## Clause B.5.4.1  Design values

The recommended value sys = 1,0 shall be used for the well defined standard testing procedures given in B.2, B.3 and B.4

## Clause D.2.2.2 (5)

No further information concerning the required density is provided in this National Annex.

# DECISION ON THE USE OF INFORMATIVE ANNEXES

## Annex B

Annex B may be used.

## Annex C

Annex C may be used.

## Annex D

Annex D may be used.

# REFERENCES TO NON-CONTRADICTORY COMPLEMENTARY INFORMATION

None