NATIONAL ANNEX

TO

CYS EN 1993-1-2:2005/AC:2009

Eurocode 3: Design of steel structures

Part 1-2: General rules – Structural fire design

DRAFT FOR PUBLIC ENQUIRY

Prepared by: CYS/TC18 EUROCODES COMMITTEE

Cyprus Organisation of Standardisation

INTRODUCTION

This National Annex has been prepared by the CYS/TC18 Committee of the Cyprus Organisation of Standardisation.

# SCOPE

This National Annex is to be used in conjunction with CYS EN 1993-1-2:2005 (Including Corrigendum AC:2009). Any reference in the rest of this text to CYS EN 1993-1-2:2005 means the above document.

This National Annex gives:

Nationally Determined Parameters described in the following clauses of CYS EN 1993-1-2:2005 (see Section NA 2):

2.3 (1)

2.3 (2)

4.1 (2)

4.2.3.6 (1)

4.2.4 (2)

Decisions on the use of CYS EN 1993-1-2:2005 informative annexes (see Section NA 3)

References to non-contradictory complementary information to assist the user to apply CYS EN 1993-1-2:2005 (see Section NA 4)

# NATIONALLY DETERMINED PARAMETERS

## Clause 2.3 (1) Design values of material properties

The value of M,fi is 1,0.

## Clause 2.3 (2) Design values of material properties

The value of M,fi is 1,0.

## Clause 4.1 (2) General

Advanced calculation models may be used at the discretion of the designer.

## Clause 4.2.3.6 (1) Members with Class 4 cross-sections

The value of crit is 350°C.

## Clause 4.2.4 (2) Critical temperature

Table 4.1 (CYS) specifies the critical temperatures a,cr for values of 0 from 0,22 to 0,80 of Table 4.1 of CYS EN 1993-1-2:2005.

| Table 4.1 (CYS): Critical temperature a,cr for values of the utilisation factor 0 |
| --- |
| 0 | a,cr | 0 | a,cr | 0 | a,cr |
| 0,22 | 711 | 0,42 | 612 | 0,62 | 549 |
| 0,24 | 698 | 0,44 | 605 | 0,64 | 543 |
| 0,26 | 685 | 0,46 | 598 | 0,66 | 537 |
| 0,28 | 674 | 0,48 | 591 | 0,68 | 531 |
| 0,30 | 664 | 0,50 | 585 | 0,70 | 526 |
| 0,32 | 654 | 0,52 | 578 | 0,72 | 520 |
| 0,34 | 645 | 0,54 | 572 | 0,74 | 514 |
| 0,36 | 636 | 0,56 | 566 | 0,76 | 508 |
| 0,38 | 628 | 0,58 | 560 | 0,78 | 502 |
| 0,40 | 620 | 0,60 | 554 | 0,80 | 496 |

# DECISION ON THE USE OF INFORMATIVE ANNEXES

## Annex C

Annex C may be used.

## Annex D

Annex D may be used.

## Annex E

Annex E may be used.

# REFERENCES TO NON-CONTRADICTORY COMPLEMENTARY INFORMATION

None