NATIONAL ANNEX

TO

CYS EN 1993-6:2007/AC:2009 Eurocode 3: Design of steel structures

Part 6: Crane supporting structures

DRAFT FOR PUBLIC ENQUIRY

Prepared by: CYS/TC18 EUROCODES COMMITTEE

Cyprus Organisation of Standardisation

INTRODUCTION

This National Annex has been prepared by the Eurocodes Committee of the Technical Chamber of Cyprus which was commissioned by the Ministry of Interior of the Republic of Cyprus

# SCOPE

This National Annex is to be used together with CYS EN 1993-6:2007

This National Annex gives:

Nationally determined parameters for the following clauses of CYS EN 1993-6:2007 where National choice is allowed (see Section NA 2)

2.1.3.2(1)P

2.8(2)P

3.2.3(1)

3.2.3(2)P

3.2.4(1) table 3.2

3.6.2(1)

3.6.3(1)

6.1(1)

6.3.2.3(1)

7.3(1)

7.5(1)

8.2(4)

9.1(2)

9.2(1)P

9.2(2)P

9.3.3(1)

9.4.2(5)

Decisions on the use of the Informative Annex A (see Section NA 3).

References to non-contradictory complementary information to assist the user to apply CYS EN 1993-6:2007 (see Section NA 4)

# NATIONALLY DETERMINED PARAMETERS

## Clause 2.1.3.2(1)P  Design working life.

The recommended design working life of 25 years shall be used for runway beams, but for runways that are not intensively used, a design working life 50 years shall be used .

## Clause 2.8(2)P  Partial factor  (F,test  for crane test loads.

The value for  the partial factor for crane loads (F,test  is specified as (F,test  = 1,1

## Clause 3.2.3(1) Lowest service temperature for indoor crane supporting structures

Refer to CYS EN1991-1-5 and its National Annex.

## Clause 3.2.3(2)P Selection of toughness properties for members in compression.

Table 2.1 (CYS) of the National Annex of CYS EN 1993-1-10 for (Ed = 0,25 fy(t) shall be used for the toughness properties, which is repeated below

Table 2.1 (CYS): Maximum permissible values of element thickness t in mm

| Steel grade | Sub-grade | Charpy energy CVN | Reference temperature TEd [°C] |
| --- | --- | --- | --- |
|  |  |  | 10 | 0 | -10 | -20 | -30 | -40 | -50 | 10 | 0 | -10 | -20 | -30 | -40 | -50 | 10 | 0 | -10 | -20 | -30 | -40 | -50 |
|  |  | at T [°C] | Jmin | (Ed = 0,75 fy(t) | (Ed = 0,50 fy(t) | (Ed = 0,25 fy(t) |
| S235 | JR | 20 | 27 | 60 | 50 | 40 | 35 | 30 | 25 | 20 | 90 | 75 | 65 | 55 | 45 | 40 | 35 | 135 | 115 | 100 | 85 | 75 | 65 | 60 |
|  | J0 | 0 | 27 | 90 | 75 | 60 | 50 | 40 | 35 | 30 | 125 | 105 | 90 | 75 | 65 | 55 | 45 | 175 | 155 | 135 | 115 | 100 | 85 | 75 |
|  | J2 | -20 | 27 | 125 | 105 | 90 | 75 | 60 | 50 | 40 | 170 | 145 | 125 | 105 | 90 | 75 | 65 | 200 | 200 | 175 | 155 | 135 | 115 | 100 |
| S275 | JR | 20 | 27 | 55 | 45 | 35 | 30 | 25 | 20 | 15 | 80 | 70 | 55 | 50 | 40 | 35 | 30 | 125 | 110 | 95 | 80 | 70 | 60 | 55 |
|  | J0 | 0 | 27 | 75 | 65 | 55 | 45 | 35 | 30 | 25 | 115 | 95 | 80 | 70 | 55 | 50 | 40 | 165 | 145 | 125 | 110 | 95 | 80 | 70 |
|  | J2 | -20 | 27 | 110 | 95 | 75 | 65 | 55 | 45 | 35 | 155 | 130 | 115 | 95 | 80 | 70 | 55 | 200 | 190 | 165 | 145 | 125 | 110 | 95 |
|  | M,N | -20 | 40 | 135 | 110 | 95 | 75 | 65 | 55 | 45 | 180 | 155 | 130 | 115 | 95 | 80 | 70 | 200 | 200 | 190 | 165 | 145 | 125 | 110 |
|  | ML,NL | -50 | 27 | 185 | 160 | 135 | 110 | 95 | 75 | 65 | 200 | 200 | 180 | 155 | 130 | 115 | 95 | 230 | 200 | 200 | 200 | 190 | 165 | 145 |
| S355 | JR | 20 | 27 | 40 | 35 | 25 | 20 | 15 | 15 | 10 | 65 | 55 | 45 | 40 | 30 | 25 | 25 | 110 | 95 | 80 | 70 | 60 | 55 | 45 |
|  | J0 | 0 | 27 | 60 | 50 | 40 | 35 | 25 | 20 | 15 | 95 | 80 | 65 | 55 | 45 | 40 | 30 | 150 | 130 | 110 | 95 | 80 | 70 | 60 |
|  | J2 | -20 | 27 | 90 | 75 | 60 | 50 | 40 | 35 | 25 | 135 | 110 | 95 | 80 | 65 | 55 | 45 | 200 | 175 | 150 | 130 | 110 | 95 | 80 |
|  | K2,M,N | -20 | 40 | 110 | 90 | 75 | 60 | 50 | 40 | 35 | 155 | 135 | 110 | 95 | 80 | 65 | 55 | 200 | 200 | 175 | 150 | 130 | 110 | 95 |
|  | ML,NL | -50 | 27 | 155 | 130 | 110 | 90 | 75 | 60 | 50 | 200 | 180 | 155 | 135 | 110 | 95 | 80 | 210 | 200 | 200 | 200 | 175 | 150 | 130 |
| S420 | M,N | -20 | 40 | 95 | 80 | 65 | 55 | 45 | 35 | 30 | 140 | 120 | 100 | 85 | 70 | 60 | 50 | 200 | 185 | 160 | 140 | 120 | 100 | 85 |
|  | ML,NL | -50 | 27 | 135 | 115 | 95 | 80 | 65 | 55 | 45 | 190 | 165 | 140 | 120 | 100 | 85 | 70 | 200 | 200 | 200 | 185 | 160 | 140 | 120 |
| S460 | Q | -20 | 30 | 70 | 60 | 50 | 40 | 30 | 25 | 20 | 110 | 95 | 75 | 65 | 55 | 45 | 35 | 175 | 155 | 130 | 115 | 95 | 80 | 70 |
|  | M,N | -20 | 40 | 90 | 70 | 60 | 50 | 40 | 30 | 25 | 130 | 110 | 95 | 75 | 65 | 55 | 45 | 200 | 175 | 155 | 130 | 115 | 95 | 80 |
|  | QL | -40 | 30 | 105 | 90 | 70 | 60 | 50 | 40 | 30 | 155 | 130 | 110 | 95 | 75 | 65 | 55 | 200 | 200 | 175 | 155 | 130 | 115 | 95 |
|  | ML,NL | -50 | 27 | 125 | 105 | 90 | 70 | 60 | 50 | 40 | 180 | 155 | 130 | 110 | 95 | 75 | 65 | 200 | 200 | 200 | 175 | 155 | 130 | 115 |
|  | QL1 | -60 | 30 | 150 | 125 | 105 | 90 | 70 | 60 | 50 | 200 | 180 | 155 | 130 | 110 | 95 | 75 | 215 | 200 | 200 | 200 | 175 | 155 | 130 |
| S690 | Q | 0 | 40 | 40 | 30 | 25 | 20 | 15 | 10 | 10 | 65 | 55 | 45 | 35 | 30 | 20 | 20 | 120 | 100 | 85 | 75 | 60 | 50 | 45 |
|  | Q | -20 | 30 | 50 | 40 | 30 | 25 | 20 | 15 | 10 | 80 | 65 | 55 | 45 | 35 | 30 | 20 | 140 | 120 | 100 | 85 | 75 | 60 | 50 |
|  | QL | -20 | 40 | 60 | 50 | 40 | 30 | 25 | 20 | 15 | 95 | 80 | 65 | 55 | 45 | 35 | 30 | 165 | 140 | 120 | 100 | 85 | 75 | 60 |
|  | QL | -40 | 30 | 75 | 60 | 50 | 40 | 30 | 25 | 20 | 115 | 95 | 80 | 65 | 55 | 45 | 35 | 190 | 165 | 140 | 120 | 100 | 85 | 75 |
|  | QL1 | -40 | 40 | 90 | 75 | 60 | 50 | 40 | 30 | 25 | 135 | 115 | 95 | 80 | 65 | 55 | 45 | 200 | 190 | 165 | 140 | 120 | 100 | 85 |
|  | QL1 | -60 | 30 | 110 | 90 | 75 | 60 | 50 | 40 | 30 | 160 | 135 | 115 | 95 | 80 | 65 | 55 | 200 | 200 | 190 | 165 | 140 | 120 | 100 |

## Clause 3.2.4(1) Requirement  ZEd  for through-thickness properties.

The allocation in Table 3.2 (CYS) is specified for crane supporting structures.

Table 3.2 (CYS) Choice of quality class according to EN 10164

| Target value of ZEd according to EN 1993-1-10 | Required value of ZRd according to EN 10164 |
| --- | --- |
| ( 10 11 to 20 21 to 30 > 30 | — Z 15 Z 25 Z 35 |

## Clause 3.6.2(1) Information on suitable rails and rail steels.

No further information on suitable rails and rail steels is provided in this National Annex.

## Clause 3.6.3(1) Information on special connecting devices for rails.

No further information on special connecting devices for rails is provided in this National Annex.

## Clause 6.1(1)  Partial factors  (Mi  for resistance for ultimate limit states.

The values for the following partial factors are  specidied as:

(M0	=	1,00

(M1	=	1,00

(M2	=	1,25

(M3	=	1,25

(M3,ser	=	1,10

(M4	=	1,00

(M5	=	1,00

(M6,ser	=	1,00

(M7	=	1,10

## Clause 6.3.2.3(1) Alternative assessment method for lateral-torsional  buckling

No further information for  alternative assessment method is specified in this National Annex.  The method given in Annex A may be used.

## Clause 7.3(1) Limits for deflections and deformations.

The limits given in Table 7.1 (CYS) are specified for horizontal deflections under the characteristic combination of actions.  The limits given in Table 7.2 (CYS) are specified for vertical deflections under the characteristic combination of actions without any dynamic amplification factors.

Table 7.1 (CYS) : Limiting values of horizontal deflections

| Description of deflection (deformation or displacement) | Diagram |
| --- | --- |
| a) Horizontal deformation y of a runway beam, measured at the level of the top of the crane rail: y ( L/600 |  |
| b) Horizontal displacement y of a frame (or of a column) at crane support level, due to crane loads: y ( hc/400 where: hc is the height to the level at which the crane is supported (on a rail or on a flange) |  |
| c) Difference y between the horizontal displacements of adjacent frames (or columns) supporting the beams of an indoor crane runway: y ( L/600 |  |
| d) Difference y between the horizontal displacements of adjacent columns (or frames) supporting the beams of an outdoor crane runway: - due to the combination of lateral crane forces and the in-service wind load: y ( L/600 - due to the out-of-service wind load y ( L/400 |  |
| e) Change of spacing s between the centres of crane rails, including the effects of thermal changes: s ( 10 mm [see Note] |  |
| Note: Horizontal deflections and deviations of crane runways are considered together in crane design. Acceptable deflections and tolerances depend on the details and clearances in the guidance means. Provided that the clearance c between the crane wheel flanges and the crane rail (or between the alternative guidance means and the crane beam) is also sufficient to accommodate the necessary tolerances, larger deflection limits can be specified for each project if agreed with the crane supplier and the client. |  |

Table 7.2 (CYS) : Limiting values of vertical deflections

| Description of deflection (deformation or displacement) | Diagram |
| --- | --- |
| a) Vertical deformation z of a runway beam: z ( L/600 and z ( 25 mm The vertical deformation z should be taken as the total deformation due to vertical loads, less the possible pre-camber, as for max in figure A1.1 of EN 1990. |  |
| b) Difference hc between the vertical deformations of two beams forming a crane runway: hc ( s/600 |  |
| c) Vertical deformation pay of a runway beam for a monorail hoist block, relative to its supports, due to the payload only: pay ( L/500 |  |

## Clause 7.5(1) Partial factor  (M,ser  for resistance for serviceability limit states.

The partial factor ( M,ser   for resistance for serviceability is specified as ( M,ser   = 1,00.

## Clause 8.2(4) Crane classes to be treated as “high fatigue”.

Classes S7 to S9 according to Annex B of EN 1991-3 are specified as the crane classes to be treated as “high fatigue”.

## Clause 9.1(2) Limit for number of cycles  C0  without a fatigue assessment.

The recommended numerical value Co = 104 shall be used.

## Clause 9.2(1)P Partial factor  (Ff  for fatigue loads.

The partial factor (Ff  for fatigue loads is specified as  (Ff  = 1,0.

## Clause 9.2(2)P Partial factors  (Mf  for fatigue resistance.

Table 3.1 (CYS) of the National Annex of CYS EN 1993-1-9 shall be used, which is repeated below

Table 3.1 (CYS) : Values for partial factors for fatigue strength

| Assessment method | Consequence of failure |
| --- | --- |
|  | Low consequence | High consequence |
| Damage tolerant | 1,00 | 1,15 |
| Safe life | 1,15 | 1,35 |

## Clause 9.3.3(1)  Crane classes where bending due to eccentricity may be neglected.

The bending stresses  (T,Ed  can be neglected for crane classes S0 to S3

## Clause 9.4.2(5) Damage equivalence factors  (dup for multiple crane operation.

The value of  (dup is equal to the values  (i  from Table 2.12 (CYS) of the National Annex of CYS EN 1991-3, which is repeated below, for a loading class  Si  as follows:

- for 2 cranes:	2 classes below the loading class of the crane with the lower loading class;

- for 3 or more cranes:	3 classes below the loading class of the crane with the lowest loading class.

Table 2.12(CYS)  — -values according to the classification of cranes

| Classes S | S0 | S1 | S2 | S3 | S4 | S5 | S6 | S7 | S8 | S9 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| normal stresses | 0,198 | 0,250 | 0,315 | 0,397 | 0,500 | 0,630 | 0,794 | 1,00 | 1,260 | 1,587 |
| shear stresses | 0,379 | 0,436 | 0,500 | 0,575 | 0,660 | 0,758 | 0,871 | 1,00 | 1,149 | 1,320 |
| NOTE 1: In determining the -values standardized spectra with a gaussian distribution of the load effects, the Miner rule and fatigue strength S-N lines with a slope m = 3 for normal stresses and m = 5 for shear stress have been used. NOTE 2: In case the crane classification is not included in the specification documents of the crane client indications are given in Annex B. |

# DECISION ON THE USE OF INFORMATIVE ANNEXES

## Annex A

Annex A may be used.

# REFERENCES TO NON-CONTRADICTORY COMPLEMENTARY INFORMATION

None