NATIONAL ANNEX

TO

CYS EN 1996-1-1:2005+A1:2012

Eurocode 6: Design of masonry structures

Part1-1: General rules for reinforced and unreinforced masonry structures

PUBLIC ENQUIRY DRAFT

PERIOD OF ENQUIRY

Prepared by: CYS/TC18 EUROCODES COMMITTEE

Cyprus Organization of Standardization

INTRODUCTION

This National Annex has been prepared by the CYS TC 18 Standardisation Technical  Committee of the Cyprus Organisation for Standardisation

# SCOPE

This National Annex is to be used together with CYS EN 1996-1-1:2005+A1:2012.Any reference in the rest of this text to CYS EN 1996-1-1:2005 means the above document.

This National Annex gives:

Nationally determined parameters for the following clauses of CYS EN 1996-1-1:2005+A1:2012 where National choice is allowed (see Section NA 2)

2.4.3(1)P

2.4.4(1)

3.2.2(1)

3.6.1.2(1)

3.6.2(3)

3.6.2(4)

3.6.2(6)

3.6.4(3)

3.7.2(2)

3.7.4(2)

4.3.3(3)

4.3.3(4)

5.5.1.3(3)

6.1.2.2(2)

6.2(2)

8.1.2(2)

8.5.2.2(2)

8.5.2.3(2)

8.6.2(1)

8.6.3(1)

Decisions on the use of the Informative Annexes A, B, C, D, E, F, G, H , I and J (see Section NA 3)

(c)  References to non-contradictory complementary information to assist the user to apply CYS EN 1996-1-1:2005+A1:2012.  In this National Annex such information is not provided (see Section NA 4).

# NATIONALLY DETERMINED PARAMETERS

## NA 2.1 Clause 2.4.3 Ultimate limit states

(1)P The recommended values (see Table 1 CYS) for the partial factor for materials, γM, used for the ultimate limit state are adopted.

Table 1 (CYS): Recommended values for the partial factor for materials, γM

| Material | M |
| --- | --- |
|  | Class |
|  | 1 | 2 | 3 | 4 | 5 |
|  | Masonry made with: |  |  |  |  |  |
| A | Units of Category I, designed mortara | 1,5 | 1,7 | 2,0 | 2,2 | 2,5 |
| B | Units of Category I, prescribed mortarb | 1,7 | 2,0 | 2,2 | 2,5 | 2,7 |
| C | Units of Category II, any mortara, b, e | 2,0 | 2,2 | 2,5 | 2,7 | 3,0 |
| D | Anchorage of reinforcing steel | 1,7 | 2,0 | 2,2 | 2,5 | 2,7 |
| E | Reinforcing steel and prestressing steel | 1,15 |
| F | Ancillary componentsc, d | 1,7 | 2,0 | 2,2 | 2,5 | 2,7 |
| G | Lintels according to EN 845-2 | 1,5 to 2,5 |
| a Requirements for designed mortars are given in EN 998-2 and EN 1996-2. b Requirements for prescribed mortars are given in EN 998-2 and EN 1996-2. c Declared values are mean values. d Damp proof courses are assumed to be covered by masonry M. e When the coefficient of variation for Category II units is not greater than 25 %. |

## NA 2.2 Clause 2.4.4 Serviceability limit states

(1) The recommended value of γΜ=1.0 for serviceability limit state is adopted.

## NA 2.3 Clause 3.2.2 Specification of masonry mortar

(1) Acceptable equivalent mixes are provided in Table 2 (CYS) below.

Table 2 (CYS): Acceptable equivalent mortar mixes-Composition and Strength

| Type of Mortar | Minimum Compressive Strength at 28 days, N/mm2 | Approximate Composition in parts by volume |
| --- | --- | --- |
|  |  | Cement | Hydrated Lime | Sand |
| M20 | 20 | To be confirmed by tests |
| M15 | 15 | 1 | 0-0.25 | 3 |
| M10 | 10 | 1 | 0.25-0.50 | 4-4.5 |
| M5 | 5 | 1 | 0.50-1.25 | 5-6 |
| M2 | 2.5 | 1 | 1.25-2.50 | 8-9 |

## NA 2.4 Clause 3.6.1.2 Characteristic compressive strength of masonry other than shell bedded masonry

(1) The characteristic compressive strength can be determined experimentally based on (i) method or using method (ii).

Table 2 (CYS): Acceptable equivalent mortar mixes-Composition and Strength

| Type of Mortar | Minimum Compressive Strength at 28 days, N/mm2 | Approximate Composition in parts by volume |
| --- | --- | --- |
|  |  | Cement | Hydrated Lime | Sand |
| M20 | 20 | To be confirmed by tests |
| M15 | 15 | 1 | 0-0.25 | 3 |
| M10 | 10 | 1 | 0.25-0.50 | 4-4.5 |
| M5 | 5 | 1 | 0.50-1.25 | 5-6 |
| M2 | 2.5 | 1 | 1.25-2.50 | 8-9 |

## NA 2.5 Clause 3.6.2 Characteristic shear strength of masonry

(3) The value of characteristic shear strength of masonry, fvk, in equation 3.5 shall not be greater than 0.065fb.

(4) The value of characteristic shear strength of masonry, fvk, in equation 3.6 shall not be greater than 0.045fb.

(6) The initial shear strength of the masonry, fvko, shall be selected from the values given in Table 3 (CYS).

Table 3 (CYS): Values of the intitial shear strength of masonry, fvko

| Masonry units | fvko (N/mm2) |
| --- | --- |
|  | General purpose mortar of the Strength Class given | Thin layer mortar (bed joint ≥ 0,5 mm and ≤ 3 mm) | Lightweight mortar |
| Clay | M10 - M20 | 0,30 | 0,30 | 0,15 |
|  | M2,5 - M9 | 0,20 |  |  |
|  | M1 - M2 | 0,10 |  |  |
| Calcium silicate | M10 - M20 | 0,20 | 0,40 | 0,15 |
|  | M2,5 - M9 | 0,15 |  |  |
|  | M1 - M2 | 0,10 |  |  |
| Aggregate concrete | M10 - M20 | 0,20 | 0,30 | 0,15 |
| Autoclaved Aerated Concrete | M2,5 - M9 | 0,15 |  |  |
| Manufactured stone and Dimensioned natural stone | M1 - M2 | 0,10 |  |  |

## NA 2.6 Clause 3.6.4 Characteristic flexural strength of masonry

(3) Where test data are not available values for the characteristic flexural strength of masonry, fkx1 and fkx2, may be taken from the recommended values given in Tables 4 (CYS) and 5 (CYS) below. The limitations given in CYS EN 1996-1-1:2005 shall be applied.

Table 4 (CYS): Values of fxk1, for plane of failure parallel to bed joints

| Masonry Unit | fxk1 (N/mm2) |
| --- | --- |
|  | General purpose mortar | Thin layer mortar | Lightweight mortar |
|  | fm < 5 N/mm2 | fm ≥ 5 N/mm2 |  |  |
| Clay | 0,10 | 0,10 | 0,15 | 0,10 |
| Calcium silicate | 0,05 | 0,10 | 0,20 | not used |
| Aggregate concrete | 0,05 | 0,10 | 0,20 | not used |
| Autoclaved aerated concrete | 0,05 | 0,10 | 0,15 | 0,10 |
| Manufactured stone | 0,05 | 0,10 | not used | not used |
| Dimensioned natural stone | 0,05 | 0,10 | 0,15 | not used |

Table 5 (CYS): Values of fxk2, for plane of failure perpendicular to bed joints

| Masonry Unit | fxk2 (N/mm2) |
| --- | --- |
|  | General purpose mortar | Thin layer mortar | Lightweight mortar |
|  | fm < 5 N/mm2 | fm ≥ 5 N/mm2 |  |  |
| Clay | 0,20 | 0,40 | 0,15 | 0,10 |
| Calcium silicate | 0,20 | 0,40 | 0,30 | not used |
| Aggregate concrete | 0,20 | 0,40 | 0,30 | not used |
| Autoclaved aerated concrete |  < 400 kg/m3 | 0,20 | 0,20 | 0,20 | 0,15 |
|  |  ( 400 kg/m3 | 0,20 | 0,40 | 0,30 | 0,15 |
| Manufactured stone | 0,20 | 0,40 | not used | not used |
| Dimensioned natural stone | 0,20 | 0,40 | 0,15 | not used |

## NA 2.7 Clause 3.7.2 Modulus of Elasticity

(2) The recommended value of KE=1000 is adopted.

## NA 2.8 Clause 3.7.4 Creep, moisture expansion or shrinkage and thermal expansion

(2) The recommended ranges of values for the deformation properties of masonry given in Table 6 (CYS) are adopted.

Table 6 (CYS): Range of coefficients of creep, moisture expansion or shrinkage, and thermal properties of masonry

| Type of masonry unit | Final creep coefficienta ( | Long term moisture expansion or shrinkageb mm/m | Coefficient of thermal expansion, αt, 10-6/K |
| --- | --- | --- | --- |
| Clay | 0,5 to 1,5 | -0,2 to +1,0 | 4 to 8 |
| Calcium Silicate | 1,0 to 2,0 | -0,4 to –0,1 | 7 to 11 |
| Dense aggregate concrete and manufactured stone | 1,0 to 2,0 | -0,6 to -0,1 | 6 to 12 |
| Lightweight aggregate concrete | 1,0 to 3,0 | -1,0 to -0,2 | 6 to 12 |
| Autoclaved aerated concrete | 0,5 to 1,5 | -0,4 to +0,2 | 7 to 9 |
| Natural stone | Magmatic | c | -0,4 to +0,7 | 5 to 9 |
|  | Sedimentary |  |  | 2 to 7 |
|  | Metamorphic |  |  | 1 to 18 |
| a The final creep coefficient ( = c( / el, where c( is the final creep strain and el =  / E. b Where the long term value of moisture expansion or shrinkage is shown as a negative number it indicates shortening and as a positive number it indicates expansion. c These values are normally very low. |

## NA 2.9 Clause 4.3.3 Reinforcing steel

(3) Recommended reinforcing steels for durability given in Table 7 (CYS) are adopted.

(4) Recommended concrete cover depth, cnom, values given in Table 8 (CYS) are adopted.

Table 7 (CYS): Selection of reinforcing steel for durability

| Exposure classa | Minimum level of protection for reinforcing steel |
| --- | --- |
|  | Located in mortar | Located in concrete with cover less than required according to (4) |
| MX1 | Unprotected carbon steelb | Unprotected carbon steel |
| MX2 | Carbon steel, heavily galvanised or with equivalent protectionc | Unprotected carbon steel or, where mortar is used to fill in the voids, carbon steel, heavily galvanised or with equivalent protectionc |
|  | Unprotected carbon steel, in masonry with a rendering mortar on the exposed face d |  |
| MX3 | Austenitic stainless steel AISI 316 or 304 | Carbon steel, heavily galvanised or with equivalent protectionc |
|  | Unprotected carbon steel, in masonry with a rendering mortar on the exposed face d |  |
| MX4 | Austenitic stainless steel AISI 316 Carbon steel heavily galvanised or with equivalent protection b with a rendering mortar on the exposed face d | Austenitic stainless steel AISI 316 |
| MX5 | Austenitic stainless steel AISI 316 or 304e | Austenitic stainless steel AISI 316 or 304e |
| a See EN 1996-2 b For the inner leaf of external cavity walls likely to become damp, carbon steel, heavily galvanised or with equivalent protection as c, should be used. c Carbon steel should be galvanised with a minimum mass of zinc coating of 900 g/m2 or galvanised with a minimum mass of zinc coating of 60 g/m2 and provided with a bonded epoxy coating of at least 80 (m thickness, with an average of 100 (m. See also 3.4. d The mortar should be general purpose or thin layer mortar, not less than M4, the side cover in figure 8.2 should be increased to 30 mm and the masonry should be rendered with a rendering mortar in accordance with EN 998-1. e Austenitic stainless steel may still not be suitable for all aggressive environments, and these should be considered on a project by project basis. |

Table 8 (CYS): Recommended values for the minimum concrete cover cnom for carbon reinforced steel

| Exposure class | Minimum cement content a kg/m3 |
| --- | --- |
|  | 275 | 300 | 325 | 350 | 400 |
|  | Maximum water/cement ratio |
|  | 0,65 | 0,60 | 0,55 | 0,50 | 0,45 |
|  | Thickness of minimum concrete cover mm |
| MX1b | 20 | 20 | 20c | 20c | 20c |
| MX2 | ( | 35 | 30 | 25 | 20 |
| MX3 | ( | ( | 40 | 30 | 25 |
| MX4 and MX5 | ( | ( | ( | 60d | 50 |
| a All mixes are based on the use of normal-weight aggregate of 20 mm nominal maximum size. Where other sized aggregates are used, cement contents should be adjusted by +20 % for 14 mm aggregate and +40 % for 10 mm aggregate. b Alternatively, a 1: 0 to ¼ : 3: 2 (cement : lime: sand : 10 mm nominal aggregate mix by volume) may be used to meet exposure situation MX1, when the cover to reinforcement is a minimum of 15 mm. c These covers may be reduced to a minimum of 15 mm provided that the nominal maximum size of the aggregate does not exceed 10 mm. d Where the concrete infill may be subjected to freezing while still wet, frost resistant concrete should be used. |

NA 2.10 Clause 5.5.1.3 Effective thickness of masonry walls

(3) The recommended value of factor ktef (defined as E1/E2) shall not be taken to be greater than 2.

## NA 2.11 Clause 6.1.2.2 Reduction factor for slenderness and eccentricity

(2) The recommended value of λc=15 is adopted.

## NA 2.12 Clause 6.2 Design value of the limiting shear resistance

(2) The equation 6.13 is adopted.

## NA 2.13 Clause 8.1.2 Minimum thickness of wall

(2) The value of tmin shall satisfy the outcome of the calculations for a robust wall that satisfies this standard, as recommended by the standard.

## NA 2.14 Clause 8.5.2.2 Cavity and veneer walls

(2) The recommended value of ntmin=2 for both cavity and veneer walls is adopted.

## NA 2.15 Clause 8.5.2.3 Double-leaf walls

(2) The recommended value of j=2 is adopted.

## NA 2.16 Clause 8.6.2 Vertical chases and recesses

(1) The recommended values for tch,v given in Table 9 (CYS) are adopted.

Table 9 (CYS): Sizes of vertical chases and recesses in masonry, tch,v , allowed without calculation

|  | Chases and recesses formed after construction of masonry | Chases and recesses formed during construction of masonry |
| --- | --- | --- |
| Thickness of wall | max depth | max width | minimum wall thickness remaining | max width |
| mm | mm | mm | mm | mm |
| 85 - 115 | 30 | 100 | 70 | 300 |
| 116 – 175 | 30 | 125 | 90 | 300 |
| 176 – 225 | 30 | 150 | 140 | 300 |
| 226 – 300 | 30 | 175 | 175 | 300 |
| > 300 | 30 | 200 | 215 | 300 |
| NOTE 1 The maximum depth of the recess or chase should include the depth of any hole reached when forming the recess or chase. NOTE 2 Vertical chases which do not extend more than one third of the storey height above floor level may have a depth up to 80 mm and a width up to 120 mm, if the thickness of the wall is 225 mm or more. NOTE 3 The horizontal distance between adjacent chases or between a chase and a recess or an opening should not be less than 225 mm. NOTE 4 The horizontal distance between any two adjacent recesses, whether they occur on the same side or on opposite sides of the wall, or between a recess and an opening, should not be less than twice the width of the wider of the two recesses. NOTE 5 The cumulative width of vertical chases and recesses should not exceed 0,13 times the length of the wall. |

## NA 2.17 Clause 8.6.3 Horizontal and inclined chases

- The recommended values for tch,h given in Table 10 (CYS) are adopted.

Table 10 (CYS): Sizes of horizontal and inclined chases in masonry, tch,h, allowed without calculation

| Thickness of wall mm | Maximum depth mm |
| --- | --- |
|  | Unlimited length | Length ≤ 1 250 mm |
| 85 - 115 | 0 | 0 |
| 116 - 175 | 0 | 15 |
| 176 - 225 | 10 | 20 |
| 226 - 300 | 15 | 25 |
| over 300 | 20 | 30 |
| NOTE 1 The maximum depth of the chase should include the depth of any hole reached when forming the chase. NOTE 2 The horizontal distance between the end of a chase and an opening should not be less than 500 mm. NOTE 3 The horizontal distance between adjacent chases of limited length, whether they occur on the same side or on opposite sides of the wall, should be not less than twice the length of the longest chase. NOTE 4 In walls of thickness greater than 115 mm, the permitted depth of the chase may be increased by 10 mm if the chase is machine cut accurately to the required depth. If machine cuts are used, chases up to 10 mm deep may be cut in both sides of walls of thickness not less than 225 mm. NOTE 5 The width of chase should not exceed half the residual thickness of the wall. |

# DECISION ON USE OF THE INFORMATIVE ANNEXES A-J

## NA 3.1 Annex A

Annex A may be used

## NA 3.2 Annex B

Annex B may be used

## NA 3.3 Annex C

Annex C may be used

## NA 3.4 Annex D

Annex D may be used

## NA 3.5 Annex E

Annex E may be used

## NA 3.6 Annex F

Annex F may be used

## NA 3.7 Annex G

Annex G may be used

## NA 3.8 Annex H

Annex H may be used

## NA 3.9 Annex I

Annex I may be used

## NA 3.10 Annex J

Annex J may be used

# REFERENCES TO NON-CONTRADICTORY COMPLEMENTARY INFORMATION

None