NATIONAL ANNEX

TO

CYS EN 1996-3:2006+AC:2009

Eurocode 6: Design of masonry structures

Part 3: Simplified calculation methods for unreinforced masonry structures

Prepared by: CYS/TC18 Eurocodes Committee

Cyprus Organization of Standardization

INTRODUCTION

This National Annex has been prepared by the CYS TC 18 Standardisation Technical Committee Eurocodes of the Cyprus Organisation for Standardisation.

# SCOPE

This National Annex is to be used together with CYS EN 1996-3:2006+AC:2009.Any reference in the rest of this text to CYS EN 1996-3:2006 means the above document.

This National Annex gives:

Nationally determined parameters for the following clauses of CYS EN 1996-3:2006+AC:2009 where National choice is allowed (see Section NA 2)

2.3(2)P

4.1(P)

4.2.1.1(1)P

4.2.2.3(1)

D.1(1)

D.2(1)

D.3(1)

Decisions on the use of the Informative Annexes A and C (see Section NA 3)

# NATIONALLY DETERMINED PARAMETERS

## Clause 2.3 Verification by the partial factor method

(2)P The relevant values of the partial factor for materials γΜ, given in clause 2.4.3 of CYS EN 1996-1-1:2005+A1:2012, shall be used for the ultimate limit state for ordinary situations.

## Clause 4.1 General

(2)P The overall stability of a building, of which the wall forms a part, shall be verified in accordance with 5.4(1) of CYS EN1996-1-1:2005+A1:2012

## Clause 4.2.1.1 General conditions for application

(1)P The numerical value to be ascribed to the symbol hm shall be taken from the table bellow.

| Class | 1 | 2 | 3 |
| --- | --- | --- | --- |
| hm | 20 m | 16 m | 12 m |

## Clause 4.2.2.3 Capacity reduction factor

(1)P The minimum number of wall ties per m2, ntmin = 2

## Clause D.1 (1) Characteristic compressive strength

The characteristic compressive strength of masonry may be calculated using the clause 3.6.1.2 of CYS EN 1996-1-1:2005+A1:2012, or from the tables bellow

Clay Units Group 1

| fb [N/mm²] | General purpose mortar | Thin joint | Light weight mortar |
| --- | --- | --- | --- |
|  | M2,5 | M5 | M10 | M20 |  | M2,5 | M5 | M10 |
| 2 4 6 8 | 1,2 1,9 2,5 3,1 | 1,4 2,4 3,1 3,8 | 1,4 2,7 3,8 4,7 | 1,4 2,7 4,1 5,4 | 1,2 2,0 2,6 3,2 | 0,6 1,0 1,4 1,7 | 0,7 1,3 1,7 2,1 | 0,7 1,5 2,1 2,6 |
| 10 12 16 20 | 3,6 4,1 5,0 5,9 | 4,5 5,1 6,2 7,3 | 5,5 6,2 7,6 8,9 | 6,8 7,7 9,4 11,0 | 3,8 4,3 5,2 6,1 | 2,0 2,2 2,8 3,2 | 2,4 2,8 3,4 4,0 | 3,0 3,4 4,2 4,9 |
| 25 30 50 75 | 6,9 7,8 11,2 14,9 | 8,5 9,6 13,8 18,3 | 10,4 11,9 17,0 22,5 | 12,9 14,6 20,9 27,7 | 7,1 8,1 11,6 11,6 | 3,8 4,3 6,1 8,1 | 4,6 5,3 7,5 10,0 | 5,7 6,5 9,3 12,3 |

Clay Units Group 2

| fb [N/mm²] | General purpose mortar | Thin joint | Light weight mortar |
| --- | --- | --- | --- |
|  | M2,5 | M5 | M10 | M20 |  | M2,5 | M5 | M10 |
| 2 4 6 8 | 1,0 1,6 2,1 2,5 | 1,1 1,9 2,6 3,1 | 1,1 2,2 3,1 3,8 | 1,1 2,2 3,3 4,4 | 1,1 1,8 2,5 3,0 | 0,5 0,9 1,2 1,4 | 0,6 1,1 1,4 1,7 | 0,6 1,2 1,7 2,1 |
| 10 12 16 20 | 3,0 3,4 4,1 4,8 | 3,7 4,2 5,1 5,9 | 4,5 5,1 6,3 7,3 | 5,5 6,3 7,7 9,0 | 3,5 4,0 4,9 5,7 | 1,6 1,9 2,3 2,7 | 2,0 2,3 2,8 3,3 | 2,5 2,8 3,5 4,1 |
| 25 30 50 75 | 5,6 6,4 9,2 12,2 | 6,9 7,9 11,3 15,0 | 8,5 9,7 13,9 18,4 | 10,5 12,0 17,1 22,7 | 6,7 7,6 10,8 10,8 | 3,1 3,6 5,1 6,8 | 3,9 4,4 6,3 8,3 | 4,7 5,4 7,7 10,2 |

Clay Units Group 3 and 4

| fb [N/mm²] | General purpose mortar | Thin joint | Light weight mortar |
| --- | --- | --- | --- |
|  | M2,5 | M5 | M10 | M20 | Group 3 | Group 4 | M2,5 | M5 | M10 |
| 2 4 6 8 | 0,7 1,2 1,6 2,0 | 0,9 1,5 2,0 2,4 | 0,9 1,7 2,4 3,0 | 0,9 1,7 2,6 3,4 | 0,8 1,3 1,8 2,1 | 0,6 1,1 1,6 2,0 | 0,4 0,7 0,9 1,1 | 0,5 0,9 1,1 1,4 | 0,5 1,0 1,4 1,7 |
| 10 12 16 20 | 2,3 2,6 3,2 3,8 | 2,8 3,2 4,0 4,6 | 3,5 4,0 4,9 5,7 | 4,3 4,9 6,0 7,0 | 2,5 2,8 3,5 4,1 | 2,5 2,9 3,7 4,5 | 1,3 1,5 1,8 2,1 | 1,6 1,8 2,3 2,6 | 2,0 2,3 2,8 3,2 |
| 25 30 50 75 | 4,4 5,0 7,1 9,5 | 5,4 6,1 8,8 11,6 | 6,6 7,6 10,8 14,3 | 8,2 9,3 13,3 17,7 | 4,8 5,4 7,7 7,7 | 5,4 6,3 9,7 9,7 | 2,5 2,8 4,1 5,4 | 3,1 3,5 5,0 6,7 | 3,8 4,3 6,2 8,2 |

Calcium silicate, aggregate concrete and autoclaved aerated concrete units Group 1

| fb [N/mm²] | General purpose mortar | Thin joint | Light weight mortar (not for calcium silicate units) |
| --- | --- | --- | --- |
|  | M2,5 | M5 | M10 | M20 |  | M2,5 | M5 | M10 |
| 2 4 6 8 | 1,2 1,9 2,5 3,1 | 1,4 2,4 3,1 3,8 | 1,4 2,7 3,8 4,7 | 1,4 2,7 4,1 5,4 | 1,4 2,6 3,7 4,7 | 1,0 1,6 2,1 2,5 | 1,1 1,9 2,6 3,1 | 1,1 2,2 3,1 3,8 |
| 10 12 16 20 | 3,6 4,1 5,0 5,9 | 4,5 5,1 6,2 7,3 | 5,5 6,2 7,6 8,9 | 6,8 7,7 9,4 11,0 | 5,7 6,6 8,4 10,2 | 3,0 3,4 4,1 4,8 | 3,7 4,2 5,1 5,9 | 4,5 5,1 6,3 7,3 |
| 25 30 50 | 6,9 7,8 11,2 | 8,5 9,6 13,8 | 10,4 11,9 17,0 | 12,9 14,6 20,9 | 12,3 14,4 22,2 | 5,6 6,4 9,2 | 6,9 7,9 11,3 | 8,5 9,7 13,9 |

Calcium silicate and aggregate concrete units Group 2

| fb [N/mm²] | General purpose mortar | Thin joint | Light weight mortar (not for calcium silicate units) |
| --- | --- | --- | --- |
|  | M2,5 | M5 | M10 | M20 |  | M2,5 | M5 | M10 |
| 2 4 6 8 | 1,0 1,6 2,1 2,5 | 1,1 1,9 2,6 3,1 | 1,1 2,2 3,1 3,8 | 1,1 2,2 3,3 4,4 | 1,1 1,7 2,3 2,8 | 1,0 1,6 2,1 2,5 | 1,1 1,9 2,6 3,1 | 1,1 2,2 3,1 3,8 |
| 10 12 16 20 | 3,0 3,4 4,1 4,8 | 3,7 4,2 5,1 5,9 | 4,5 5,1 6,3 7,3 | 5,5 6,3 7,7 9,0 | 3,3 3,7 4,5 5,3 | 3,0 3,4 4,1 4,8 | 3,7 4,2 5,1 5,9 | 4,5 5,1 6,3 7,3 |
| 25 30 50 | 5,6 6,4 9,2 | 6,9 7,9 11,3 | 8,5 9,7 13,9 | 10,5 12,0 17,1 | 6,2 7,0 10,1 | 5,6 6,4 9,2 | 6,9 7,9 11,3 | 8,5 9,7 13,8 |

Aggregate concrete units Group 3

| fb [N/mm²] | General purpose mortar | Thin joint |
| --- | --- | --- |
|  | M2,5 | M5 | M10 | M20 |  |
| 2 4 6 8 | 0,9 1,4 1,8 2,3 | 1,0 1,7 2,3 2,8 | 1,0 2,0 2,8 3,4 | 1,0 2,0 3,0 3,9 | 0,8 1,3 1,8 2,1 |
| 10 12 16 20 | 2,6 3,0 3,7 4,3 | 3,2 3,7 4,5 5,3 | 4,0 4,5 5,6 6,5 | 4,9 5,6 6,8 8,0 | 2,5 2,8 3,5 4,1 |
| 25 30 50 | 5,0 5,7 8,1 | 6,2 7,0 10,0 | 7,6 8,6 12,3 | 9,4 10,6 15,2 | 4,8 5,4 7,7 |

The use of the above tables is allowed taking into account that:

- CYS-EN 998-2 gives no limit for the thickness of joints made of thin layer mortar; the values in the above tables are based on a thickness of 0.5 - 3 mm to ensure that the thin layer mortar has the enhanced properties required to achieve the given values.

- The thickness of the masonry is equal to the width or length of the unit, so that there is no mortar joint parallel to the face of the wall through all or any part of the length of the wall.

- The coefficient of variation of the strength of the masonry units is not more than 25 %.

- Where action effects are parallel to the direction of the bed joints, the characteristic compressive strength may also be determined from the tables, using the normalised compressive strength of the masonry unit, fb, obtained from tests where the direction of application of the load to the test specimen is the same as the direction of the action effect in the masonry, but with the factor, (, as given in EN 772,Annex A, not taken to be greater than 1,0. For Group 2 and 3 units, the value of fk obtained from the tables should be multiplied by 0,5.

- For masonry made of general purpose mortar where Group 2 and Group 3 aggregate concrete units are used with the vertical cavities filled completely with concrete, the value of fb should be obtained by considering the units to be Group 1 with a compressive strength corresponding to the compressive strength of the units or of the concrete infill, whichever is the lesser.

- When the perpendicular joints are unfilled, the tables may be used, with due consideration being given to any horizontal actions that might be applied to, or be transmitted by, the masonry.

- For masonry made with general purpose mortar where there is a mortar joint parallel to the face of the wall through all, or any part, of the length of the wall, the values of fk can be obtained by multiplying the values given in the tables by 0,8.

## Clause D.2 (1) Characteristic flexural strength

The characteristic flexural strength of masonry may be calculated using the clause 3.6.3(2) of CYS-EN 1996-1-1:2005+A1:2012, or from the tables bellow

| Masonry unit | fxk1,s [N/mnm²] |
| --- | --- |
|  | General purpose mortar | Thin layer mortar | Light weight mortar |
|  | < M5 | ( M5 |  |  |
| Clay | 0,10 | 0,10 | 0,15 | 0,10 |
| Calcium silicate | 0,05 | 0,10 | 0,20 | not used |
| Aggregate concrete | 0,05 | 0,10 | 0,20 | not used |
| Autoclaved aerated concrete | 0,05 | 0,10 | 0,15 | 0,10 |

| Masonry unit | fxk2,s [N/mnm²] |
| --- | --- |
|  | General purpose mortar | Thin layer mortar | Light weight mortar |
|  | < M5 | ( M5 |  |  |
| Clay | 0,20 | 0,40 | 0,15 | 0,10 |
| Calcium silicate | 0,20 | 0,40 | 0,30 | not used |
| Aggregate concrete | 0,20 | 0,40 | 0,30 | not used |
| Autoclaved aerated concrete | ( < 400 kg/m³ | 0,20 | 0,20 | 0,20 | 0,15 |
|  | ( ( 400 kg/m³ | 0,20 | 0,40 | 0,30 | 0,15 |

- Provided that thin layer mortar and light weight mortars are M5, or stronger;

- For masonry made with autoclaved aerated concrete units laid in thin layer mortar, fxk1 and fxk2 values may be taken from the above tables or from the following equations:

fxk1,s = 0,035 fb , with filled and unfilled perpend joints;

fxk2,s = 0,035 fb , with filled perpend joints or 0,025 fb , with unfilled perpend joints.

## Clause D.3 (1) Characteristic initial shear strength

The characteristic initial shear strength of masonry fvko,s, provided  that general purpose mortars made according to CYS-EN1996-2 do not contain admixtures or additives, may be taken from the table bellow.

| Masonry unit | fvko,s [N/mnm²] |
| --- | --- |
|  | General purpose mortar of Strength Class given | Thin layer mortar | Light weight mortar |
| Clay | M1 – M2 M2,5 – M9 M10 –M20 | 0,10 0,20 0,30 | 0,30 | 0,15 |
| Calcium silicate | M1 – M2 M2,5 – M9 M10 –M20 | 0,10 0,15 0,20 | 0,40 | 0,15 |
| Aggregate concrete Autoclaved aerated concrete | M1 – M2 M2,5 – M9 M10 –M20 | 0,10 0,15 0,20 | 0,30 | 0,15 |

# DECISION ON USE OF ANNEXES A AND C

## Annex A

Annex A may be used

## Annex C

Annex C may be used

# REFERENCES TO NON-CONTRADICTORY COMPLEMENTARY INFORMATION

None.