# NATIONAL ANNEX

# TO

# CYS EN 1993-1-1:2022 Eurocode 3: Design of steel structures

# Part 1-1: General rules and rules for buildings

For Public Enquiry - April 2, 2026

Prepared by: CYS TC 18 EUROCODES

Cyprus Organisation for Standardisation (CYS)

INTRODUCTION

This National Annex has been prepared by the CYS TC 18: Eurocodes National Standardisation Technical Committee of Cyprus Organisation for Standardisation. (CYS)

# SCOPE

This National Annex is to be used together with CYS EN 1993-1-1:2022

This National Annex gives:

Nationally determined parameters for the following clauses of CYS EN 1993-1-1:2022 where National choice is allowed (see Section NA 2)

- 4.4.3 (2)

- 5.1 (1)

- 5.2.1 (1)

- 5.2.2 (1)

- 7.2.1 (4)

- 7.2.2 (9)

- 7.3.3.1 (1)

- 7.3.3.2 (1)

- 7.4.1 (3)

- 8.1 (1)

- 8.2.8 (3)

- 8.3.2.3 (1)

- 8.3.3 (2)

- 8.3.4 (1)

- 9.2 (2)B

- A.4 (2)

- A.4 (3)

- A.4 (5)

Decision on the use of the Informative Annex E (see Section NA 3).

References to non-contradictory complementary information to assist the user to apply CYS EN 1993-1-1:2022. In this National Annex such information is provided for the following clauses in CYS EN 1993-1-1:2022 (see Section NA 4).

# NATIONALLY DETERMINED PARAMETERS

## Clause 4.4.3(2) Design values of geometrical properties

No provisions are given for the calculation of fillet radius.

## Clause 5.1 (1) General

No other steel materials and products are given.

## Clause 5.2.1 (1) Material properties

Approach b) shall be used. The nominal values of the yield strength fy and the ultimate tensile strength fu for structural steel are given in Table 5.1(CYS) for steel conforming to EN 10025 (all parts), EN 10210 (all parts) and EN 10219 (all parts), and in Table 5.2 (CYS) for steel conforming to EN 10149 (all parts). No rules are provided for the use of the steels according to Table 5.1 (CYS) and Table 5.2 (CYS) are provided.

Table 5.1(CYS) — Nominal values of yield strength fy and ultimate tensile strength fu for structural steels conforming to the following standards: EN 10025 (all parts), EN 10210 (all parts), and EN 10219 (all parts)

| Steel gradea | Nominal thickness of the element t mm |  |  |  |
| --- | --- | --- | --- | --- |
|  | t ≤ 40 mm |  | 40 mm < t ≤ 80 mm |  |
|  | fy N/mm2 | fu N/mm2 | fy N/mm2 | fu N/mm2 |
| S235 | 235 | 360 | 215 | 360 |
| S275 | 275 | 390 | 245 | 370 |
| S355 | 355 | 490 | 325 | 470 |
| S420 | 420 | 510 | 390 | 490 |
| S460 | 460 | 540 | 410 | 510 |
| S500 | 500 | 580 | 450 | 580 |
| S550 | 550 | 600 | 500 | 600 |
| S600 | 600 | 650 | 550 | 650 |
| S620 | 620 | 700 | 560 | 660 |
| S650 | 650 | 700 | - | - |
| S690 | 690 | 770 | 630 | 710 |
| S700 | 700 | 750 | - | - |
| a Principal symbols in EN 10027-1. |  |  |  |  |

Table 5.2 (CYS) — Nominal values of yield strength fy and ultimate tensile strength fu for hot rolled flat products for cold-forming, according to EN 10149-2 and EN 10149-3

| Standards, Grades and quality | Nominal thickness of the element t mm |  |  |  |
| --- | --- | --- | --- | --- |
|  | t ≤ 8 mm |  | 8 mm < t ≤ 20 mm |  |
|  | fy N/mm2 | fu N/mm2 | fy N/mm2 | fu N/mm2 |
| EN 10149-2a |  |  |  |  |
| S315MC | 315 | 390 | 315 | 390 |
| S355MC | 355 | 430 | 355 | 430 |
| S420MC | 420 | 480 | 420 | 480 |
| S460MC | 460 | 520 | 460 | 520 |
| S500MC | 500 | 550 | 500b | 550b |
| S550MC | 550 | 600 | 550b | 600b |
| S600MC | 600 | 650 | 600b | 650b |
| S650MC | 650 | 700 | 630b | 700b |
| S700MC | 700 | 750 | 680b | 750b |
| EN 10149-3a |  |  |  |  |
| S260NC | 260 | 370 | 260 | 370 |
| S315NC | 315 | 430 | 315 | 430 |
| S355NC | 355 | 470 | 355 | 470 |
| S420NC | 420 | 530 | 420 | 530 |
| a Verification of the impact energy in accordance with EN 10149-1:2013, Clause 11, option 5 should be specified. b t ≤ 16 mm |  |  |  |  |

## Clause 5.2.2 (1) Ductility requirements

The limiting values are the following:

a)	For plastic global analysis

—

—	elongation at failure not less than 15 %.

b)	For elastic global analysis

—

—	elongation at failure not less than 12 %.

## Clause 7.2.1 (4) Consideration of second order effects

The value of k0 is 25.

## Clause 7.2.2 (9) Methods of analysis for ultimate limit state design checks

No limitations on the use of Method EM are given.

## Clause 7.3.3.1 (1) Flexural buckling

The equivalent bow imperfection, e0, of members for flexural buckling is determined according to Formula (7.9).

(7.9)

where

| L | is the member length; |
| --- | --- |
| α | is the imperfection factor, depending on the relevant buckling curve according to Table 8.2; |
| ε | is the material parameter defined in 5.2.5(2); |
| β | is the reference relative bow imperfection according to Table 7.1.(CYS) |

## Clause 7.3.3.2 (1) Lateral torsional buckling

The values of e0,LT are determined according to Formula (7.11).

where

| L | is the member length; |
| --- | --- |
| ε | is the material parameter defined in 5.2.5(2); |
| βLT | is the reference relative bow imperfection for lateral torsional buckling according to Table 7.2. |

## Clause 7.4.1(3) Methods of analysis considering material non- linearities

No rules for plastic global analysis based on plastic hinges for steel grades higher than S460 are defined.

## Clause 8.1 (1) Partial factors

The partial factors γMi for buildings are:

γM0 = 1,00

γM1 = 1,05 (option b in 5.2.1(1) is adopted so the partial factor is increased to 1,05)

γM2 = 1,25

## Clause 8.2.8 (3) Combined bending and shear

The value of ηV is 0,5.

## Clause 8.3.2.3 (1) Reduction factors χLT for lateral torsional buckling

The limiting value λLT,0 is set to 0,4. No limitations of validity concerning the beam depth or h/b ratio and the limiting value  λLT,0  are set.

## Clause 8.3.3 (2) Uniform members in bending and axial compression

CEN/TS 1993 1 101 CEN/TS 1993-1-101 is not an alternative.

## Clause 8.3.4 (1) General method for lateral and lateral torsional buckling of structural components

No further details are given for the field and limits of application of the method given in 8.3.4.

## Clause 9.2 (2)B Deformations and dynamic effects for buildings

No limits for deformation and vibration of floors are given by the National Annex.

## Clause A.4 (2) Selection process

No choice in terms of the type of the structure is given.

## Clause A.4 (3) Selection process

The selection of execution class (EXC) based on type of loading is as given in Table A.1(CYS)

Table A.1 (CYS)— Selection of execution class based on the type of loading (EXC)

| Consequence class (CC) | Type of loading |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
|  | Static Quasi-static | Seismic |  |  | Fatigueb |
|  |  | DC1a | DC2a | DC3a |  |
| CC3 | EXC3c | EXC3c | EXC3c | EXC3c | EXC3c |
| CC2 | EXC2 | EXC2 | EXC2 | EXC3d | EXC3 |
| CC1 | EXC1 | EXC2e | EXC2 | EXC2 | EXC2 |
| a Seismic ductility classes (DC’s) are defined in prEN 1998-1-1. b See EN 1993-1-9. c EXC4 may be considered for special cases, including those typically covered by CC4 of EN 1990:—. d Only the primary seismic resisting system falls in EXC3; the gravity load resisting system may fall in EXC2. e If the seismic action index is not greater than 2,5m/s2 (low seismic action class, see prEN 1998-1-1), the execution class of structures in DC1 may be EXC1. NOTE Structures in consequence class CC0 are not covered by this Annex, see EN 1990:—, 4.3. |  |  |  |  |  |

## Clause A.4 (5) Selection process

No different choices of execution class for types of components or details are given.

# DECISION ON USE OF THE INFORMATIVE ANNEX E

## Annex E

Annex E may be used

# REFERENCES TO NON-CONTRADICTORY COMPLEMENTARY INFORMATION

None