NATIONAL ANNEX

TO

CYS EN 1993-1-2:2024

Eurocode 3: Design of steel structures

Part 1-2: Structural fire design

For Public Enquiry– 2 April 2026

Prepared by: CYS TC 18 EUROCODES

Cyprus Organisation for Standardisation (CYS)

INTRODUCTION

This National Annex has been prepared by the CYS TC 18: Eurocodes National Standardisation Technical Committee of Cyprus Organisation for Standardisation. (CYS)

# SCOPE

This National Annex is to be used together with CYS EN 1993-1-2:2024

This National Annex gives:

Nationally determined parameters for the following clauses of CYS EN 1993-1-2:2024 where National choice is allowed (see Section NA 2)

4.5(1)

4.7(2)

7.5(2)

Decisions on the use of the Informative Annexes (see Section NA 3)

References to non-contradictory complementary information to assist the user to apply CYS EN 1993-1-2:2024. In this National Annex such information is provided for the following clauses in CYS EN 1993-1-2:2024 (see Section NA 4)

# NATIONALLY DETERMINED PARAMETERS

## Clause 4.5 (1) Design values of material properties

The value of γM,fi is 1,0.

## Clause 4.7 (2) Member analysis

The value of ηfi is 0,65, except for imposed loads according to category E as given in CYS EN 1990 (areas susceptible to accumulation of goods, including access areas) where the value of ηfi is 0,7.

## Clause 7.5 (2) Critical temperature

No default values are set.

For members with class 4 cross-sections, the default critical temperature, θa,cr, is equal to 350 C.

# DECISION ON THE USE OF THE INFORMATIVE ANNEXES

Not applicable.

# REFERENCES TO NON-CONTRADICTORY COMPLEMENTARY INFORMATION

None